This Product MasterSpec Section is licensed by ARCOM to Moxie International ("Licensee").

This Product MasterSpec Section modifies the original MasterSpec text, and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, ARCOM or The American Institute of Architects (AIA).  Neither AIA nor ARCOM are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user.  A qualified design professional should review and edit the document to suit project requirements.

For more information, contact Moxie International, PO Box 838, 3201 Swetzer Road, Loomis, CA 95650;                    Phone: 888.680.7303  | 916.259.7990; Fax: 877.330.1930; Website: www.moxieshield.com; Email: info@moxieshield.com.

For information about MasterSpec contact ARCOM at (800) 424-5080 or visit www.MasterSpec.com.

Copyright 2014 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 033000 - CAST-IN-PLACE CONCRETE

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section includes cast-in-place concrete, including formwork, reinforcement, concrete materials, admixtures, mixture design, placement procedures, topical treatments and finishes.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 033300 "Architectural Concrete" for general building applications of specially finished formed concrete.

          - Section 035300 "Concrete Topping" for emery- and iron-aggregate concrete floor toppings.

          - Section 312000 "Earth Moving" for drainage fill under slabs-on-grade.

          - Section 321313 "Concrete Paving" for concrete pavement and walks.

          - Section 321316 "Decorative Concrete Paving" for decorative concrete pavement and walks.

      - DEFINITIONS

Retain terms that remain after this Section has been edited for a project.

Definition in "Cementitious Materials" Paragraph below refers to those materials that make up the cementitious component of the w/c ratio.

        - Cementitious Materials: Portland cement alone or in combination with one or more of the following: blended hydraulic cement, fly ash, slag cement, other pozzolans, and silica fume; materials subject to compliance with requirements.

        - W/C Ratio: The ratio by weight of water to cementitious materials.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

Retain first subparagraph below if warranted by complexity of design mixtures and quality control of concrete materials.

          - Before submitting design mixtures, review concrete design mixture and examine procedures for ensuring quality of concrete materials. Require representatives of each entity directly concerned with cast-in-place concrete to attend, including the following:

            - Contractor's superintendent.

            - Independent testing agency responsible for concrete design mixtures.

            - Ready-mix concrete manufacturer.

            - Concrete Subcontractor.

Retain first subparagraph below if special concrete finishes are included in Project.

            - Special concrete finish Subcontractor.

          - Review [special inspection and testing and inspecting agency procedures for field quality control,] [concrete finishes and finishing,] [cold- and hot-weather concreting procedures,] [curing procedures,] [construction contraction and isolation joints, and joint-filler strips,] [semirigid joint fillers,] [forms and form removal limitations,] [shoring and reshoring procedures,] [vapor-retarder installation,] [anchor rod and anchorage device installation tolerances,] [steel reinforcement installation,] [methods for achieving specified floor and slab flatness and levelness] [floor and slab flatness and levelness measurement,] [concrete repair procedures,] and concrete protection.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

        - Sustainable Design Submittals:

          - Product Data: For recycled content, indicating postconsumer and preconsumer recycled content and cost.

          - Product Certificates: For regional materials, indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include distance to Project and cost for each regional material.

          - Laboratory Test Reports: For [liquid floor treatments] [and] [curing and sealing compounds], indicating compliance with requirements for low-emitting materials.

Design mixtures in "Design Mixtures" Paragraph below are usually considered to be an action submittal.

        - Design Mixtures: For each concrete mixture. Submit alternate design mixtures when characteristics of materials, Project conditions, weather, test results, or other circumstances warrant adjustments.

          - Indicate amounts of mixing water to be withheld for later addition at Project site.

        - Steel Reinforcement Shop Drawings: Placing Drawings that detail fabrication, bending, and placement. Include bar sizes, lengths, material, grade, bar schedules, stirrup spacing, bent bar diagrams, bar arrangement, splices and laps, mechanical connections, tie spacing, hoop spacing, and supports for concrete reinforcement.

        - Construction Joint Layout: Indicate proposed construction joints required to construct the structure.

          - Location of construction joints is subject to approval of the Architect.

        - Samples: For [waterstops] [vapor retarder] <Insert products>.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as supplemented in "Quality Assurance" Article.

        - Qualification Data: For [Installer] [manufacturer] [testing agency].

Retain "Welding certificates" Paragraph below if retaining "Welding Qualifications" Paragraph in "Quality Assurance" Article.

        - Welding certificates.

Retain "Material Certificates" Paragraph below to require submittal of material certificates from manufacturers.

        - Material Certificates: For each of the following, signed by manufacturers:

Revise fourteen subparagraphs below to suit Project.

          - Cementitious materials.

          - Admixtures.

          - Form materials and form-release agents.

          - Steel reinforcement and accessories.

          - Fiber reinforcement.

          - Waterstops.

          - Curing compounds.

          - Floor and slab treatments.

          - Bonding agents.

          - Adhesives.

          - Vapor retarders.

          - Semirigid joint filler.

          - Joint-filler strips.

          - Repair materials.

Retain "Material Test Reports" Paragraph below for material test reports that are Contractor's responsibility.

        - Material Test Reports: For the following, from a qualified testing agency:

Retain option in "Aggregates" Subparagraph below if retaining service record data with "Normal-Weight Aggregates" Paragraph in Part 2 "Concrete Materials" Article.

          - Aggregates[: Include service record data indicating absence of deleterious expansion of concrete due to alkali aggregate reactivity].

        - Formwork Shop Drawings: Prepared by or under the supervision of a qualified professional engineer, detailing fabrication, assembly, and support of formwork.

          - Shoring and Reshoring: Indicate proposed schedule and sequence of stripping formwork, shoring removal, and reshoring installation and removal.

Retain first paragraph below if Contractor engages testing agency for measuring floor surface flatness and levelness.

        - Floor surface flatness and levelness measurements indicating compliance with specified tolerances.

Retain "Field quality-control reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting.

        - Field quality-control reports.

Retain paragraph below if preinstallation conference is held.

        - Minutes of preinstallation conference.

      - QUALITY ASSURANCE

Retain "Installer Qualifications" Paragraph below if required. See Section 014000 "Quality Requirements" for general installer qualifications. Verify availability of qualified personnel with a local ACI chapter or concrete contractors. These desirable programs may have limited grass-roots penetration.

        - Installer Qualifications: A qualified installer who employs on Project personnel qualified as ACI-certified Flatwork Technician and Finisher and a supervisor who is an ACI-certified Concrete Flatwork Technician.

        - Manufacturer Qualifications: A firm experienced in manufacturing ready-mixed concrete products and that complies with ASTM C 94/C 94M requirements for production facilities and equipment.

Retain subparagraph below if required.

          - Manufacturer certified according to NRMCA's "Certification of Ready Mixed Concrete Production Facilities."

Retain "Testing Agency Qualifications" Paragraph below if Contractor retains testing agency for concrete mixture design, material test reports, or field quality control. Retain option if field quality-control testing agency employed by Contractor must be approved by authorities having jurisdiction.

        - Testing Agency Qualifications: An independent agency,[ acceptable to authorities having jurisdiction,] qualified according to ASTM C 1077 and ASTM E 329 for testing indicated.

Retain first subparagraph below, required by ACI 301 (ACI 301M) and ASTM C 31/C 31M, if emphasis is needed. ASTM C 1077 notes relevant field or laboratory technician certification by ACI, NRMCA, and Portland Cement Association; or the National Institute for Certification in Engineering Technologies may demonstrate evidence of competence.

          - Personnel conducting field tests shall be qualified as ACI Concrete Field Testing Technician, Grade 1, according to ACI CP-1 or an equivalent certification program.

Retain subparagraph below if requiring minimum qualifications for laboratory personnel performing testing and for laboratory supervisor.

          - Personnel performing laboratory tests shall be ACI-certified Concrete Strength Testing Technician and Concrete Laboratory Testing Technician, Grade I. Testing agency laboratory supervisor shall be an ACI-certified Concrete Laboratory Testing Technician, Grade II.

Retain "Welding Qualifications" Paragraph below if shop or field welding is required. If retaining, also retain "Welding certificates" Paragraph in "Informational Submittals" Article. AWS states that welding qualifications remain in effect indefinitely unless welding personnel have not welded for more than six months or there is a specific reason to question their ability.

        - Welding Qualifications: Qualify procedures and personnel according to AWS D1.4/D 1.4M.

Retain "Mockups" Paragraph below if required. If retaining, indicate location, concrete type, and other details of mockups on Drawings or by inserts. Revise wording if only one mockup is required or if mockup of concrete in another location in a building is required.

        - Mockups: Cast concrete [slab-on-grade] [and] [formed-surface] panels to demonstrate typical joints, surface finish, texture, tolerances, floor treatments, and standard of workmanship.

Revise size of panel in first subparagraph below if required. Panel for slab-on-grade may need to be enlarged if powered riding trowels are used and if it is a portion of the floor slab.

          - Build panel approximately [200 sq. ft. (18.6 sq. m) for slab-on-grade] [and] [100 sq. ft. (9.3 sq. m) for formed surface] <Insert area> in the location indicated or, if not indicated, as directed by Architect.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - PRECONSTRUCTION TESTING

        - Preconstruction Testing Service: Engage a qualified testing agency to perform preconstruction testing on concrete mixtures.

      - DELIVERY, STORAGE, AND HANDLING

Retain option in "Steel Reinforcement" Paragraph below if zinc- or epoxy-coated steel reinforcement is required.

        - Steel Reinforcement: Deliver, store, and handle steel reinforcement to prevent bending and damage.[ Avoid damaging coatings on steel reinforcement.]

        - Waterstops: Store waterstops under cover to protect from moisture, sunlight, dirt, oil, and other contaminants.

      - FIELD CONDITIONS

        - Cold-Weather Placement: Comply with ACI 306.1 and as follows. Protect concrete work from physical damage or reduced strength that could be caused by frost, freezing actions, or low temperatures.

          - When average high and low temperature is expected to fall below 40 deg F (4.4 deg C) for three successive days, maintain delivered concrete mixture temperature within the temperature range required by ACI 301 (ACI 301M).

          - Do not use frozen materials or materials containing ice or snow. Do not place concrete on frozen subgrade or on subgrade containing frozen materials.

          - Do not use calcium chloride, salt, or other materials containing antifreeze agents or chemical accelerators unless otherwise specified and approved in mixture designs.

        - Hot-Weather Placement: Comply with ACI 301 (ACI 301M) and as follows:

          - Maintain concrete temperature below 90 deg F (32 deg C) at time of placement. Chilled mixing water or chopped ice may be used to control temperature, provided water equivalent of ice is calculated to total amount of mixing water. Using liquid nitrogen to cool concrete is Contractor's option.

          - Fog-spray forms, steel reinforcement, and subgrade just before placing concrete. Keep subgrade uniformly moist without standing water, soft spots, or dry areas.

        - Penetrating Sealer Ambient Conditions:

          - Do not apply in rain.

          - Do not apply if the ambient temperature is below 50 deg F (10 deg C).

          - Do not apply in windy conditions.

      - WARRANTY

When warranties are required, verify with Owner's counsel that warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

        - Manufacturer's Warranty: Integral waterproofing admixture manufacturer agrees to repair, replace or re-apply damaged floor covering or adhesive, surface treatment, coating or paint materials that fail within specified warranty period.

          - Material Warranty Period: 40 years from date of Substantial Completion.

          - Warrantied failures include proven claims made on any floor covering or adhesive, surface treatment, coating or paint that sustains damage due to moisture vapor migration or alkali efflorescence attack, which had migrated through concrete, and includes blistering, peeling, leakage, seepage, or absorption of moisture, petroleum, sulfides, or acids.

Warrantied remedies include repairing, replacing, or re-applying floor covering or adhesive, surface treatment, coating or paint, remove any contaminants, petroleum or oil and provide the necessary labor and related materials, re-seal or re-treat the concrete and remedy the claim to the satisfaction of the original registered owner or current owner.

          - Warranty does not apply to, or cover:

            - Water vapor migration moving laterally under a floor covering originating from external sources such as drains or broken pipes.

            - Conditions resulting from materials or surface compounds, that have been prematurely applied prior to complete concrete hydration, which may impede proper concrete hydration and affect accurate testing results.

            - Structural cracks or damage or conditions caused by neglect, abuse, acts of God or nature, other materials and/or conditions resulting from inferior application or workmanship, whether intentional or not, or situations beyond its control.

            - Liquidated, incidental and/or consequential damages or for contribution or indemnity.

- PRODUCTS

Manufacturers and products listed in SpecAgent and Masterworks Paragraph Builder are neither recommended nor endorsed by the AIA or ARCOM. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - CONCRETE, GENERAL

        - ACI Publications: Comply with the following unless modified by requirements in the Contract Documents:

          - ACI 301 (ACI 301M).

          - ACI 117 (ACI 117M).

      - FORM-FACING MATERIALS

        - Smooth-Formed Finished Concrete: Form-facing panels that provide continuous, true, and smooth concrete surfaces. Furnish in largest practicable sizes to minimize number of joints.

Retain first subparagraph below if generic specification is sufficient; revise to suit Project.

          - Plywood, metal, or other approved panel materials.

          - Exterior-grade plywood panels, suitable for concrete forms, complying with DOC PS 1, and as follows:

Retain one of first four subparagraphs below or revise to suit Project. First subparagraph imparts glossy finish, second imparts matte finish, and third and fourth impart coarser-textured finish, depending on face-ply characteristics.

            - High-density overlay, Class 1 or better.

            - Medium-density overlay, Class 1 or better; mill-release agent treated and edge sealed.

            - Structural 1, B-B or better; mill oiled and edge sealed.

            - B-B (Concrete Form), Class 1 or better; mill oiled and edge sealed.

          - Overlaid Finnish birch plywood.

        - Rough-Formed Finished Concrete: Plywood, lumber, metal, or another approved material. Provide lumber dressed on at least two edges and one side for tight fit.

Forms in "Forms for Cylindrical Columns, Pedestals, and Supports" Paragraph below leave joint impressions in spiral or straight lines. Limit types of forms if a particular pattern of joint is required. Different release treatments of forms also affect appearance of as-cast surfaces.

        - Forms for Cylindrical Columns, Pedestals, and Supports: Metal, glass-fiber-reinforced plastic, paper, or fiber tubes that produce surfaces with gradual or abrupt irregularities not exceeding specified formwork surface class. Provide units with sufficient wall thickness to resist plastic concrete loads without detrimental deformation.

        - Pan-Type Forms: Glass-fiber-reinforced plastic or formed steel, stiffened to resist plastic concrete loads without detrimental deformation.

Retain void forms, sometimes called "carton forms," in "Void Forms" Paragraph below if required for expansive soils or block outs.

        - Void Forms: Biodegradable paper surface, treated for moisture resistance, structurally sufficient to support weight of plastic concrete and other superimposed loads.

Retain "Chamfer Strips" Paragraph below if chamfering is permitted.

        - Chamfer Strips: Wood, metal, PVC, or rubber strips, 3/4 by 3/4 inch (19 by 19 mm), minimum.

        - Rustication Strips: Wood, metal, PVC, or rubber strips, kerfed for ease of form removal.

        - Form-Release Agent: Commercially formulated form-release agent that does not bond with, stain, or adversely affect concrete surfaces and does not impair subsequent treatments of concrete surfaces.

          - Formulate form-release agent with rust inhibitor for steel form-facing materials.

        - Form Ties: Factory-fabricated, removable or snap-off glass-fiber-reinforced plastic or metal form ties designed to resist lateral pressure of fresh concrete on forms and to prevent spalling of concrete on removal.

Revise three subparagraphs below to suit Project; delete if not required.

          - Furnish units that leave no corrodible metal closer than 1 inch (25 mm) to the plane of exposed concrete surface.

          - Furnish ties that, when removed, leave holes no larger than 1 inch (25 mm) in diameter in concrete surface.

          - Furnish ties with integral water-barrier plates to walls indicated to receive dampproofing or waterproofing.

      - STEEL REINFORCEMENT

        - Recycled Content of Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] [60] <Insert value> percent.

        - Reinforcing Bars: ASTM A 615/A 615M, Grade 60 (Grade 420), deformed.

Retain "Low-Alloy-Steel Reinforcing Bars" Paragraph below for reinforcement that is welded or if added ductility is sought.

        - Low-Alloy-Steel Reinforcing Bars: ASTM A 706/A 706M, deformed.

Retain "Galvanized Reinforcing Bars" Paragraph below for galvanized-steel reinforcement. Retain type of reinforcement from first set of options and zinc coating class from second set. Class I has at least 50 percent more zinc weight than Class II.

        - Galvanized Reinforcing Bars: [ASTM A 615/A 615M, Grade 60 (Grade 420)] [ASTM A 706/A 706M], deformed bars, ASTM A 767/A 767M, [Class I] [Class II] zinc coated after fabrication and bending.

Retain "Epoxy-Coated Reinforcing Bars" Paragraph below for epoxy-coated steel reinforcement. Retain type of reinforcement from first set of options and epoxy-coated product from second set. ASTM A 775/A 775M bars are usually epoxy coated before fabrication; ASTM A 934/A 934M bars are epoxy coated after fabrication and should not be field bent or rebent.

        - Epoxy-Coated Reinforcing Bars: [ASTM A 615/A 615M, Grade 60 (Grade 420)] [ASTM A 706/A 706M], deformed bars, [ASTM A 775/A 775M] [or] [ASTM A 934/A 934M], epoxy coated, with less than 2 percent damaged coating in each 12-inch (300-mm) bar length.

Retain "Stainless-Steel Reinforcing Bars" Paragraph below for stainless-steel reinforcement. Retain one of two options for reinforcement type.

        - Stainless-Steel Reinforcing Bars: ASTM A 955/A 955M, Grade 60 (Grade 420), [Type 304] [Type 316L], deformed.

        - Steel Bar Mats: ASTM A 184/A 184M, fabricated from [ASTM A 615/A 615M, Grade 60 (Grade 420)] [ASTM A 706/A 706M], deformed bars, assembled with clips.

        - Plain-Steel Wire: ASTM A 1064/A 1064M, [as drawn] [galvanized].

        - Deformed-Steel Wire: ASTM A 1064/A 1064M.

        - Epoxy-Coated Wire: ASTM A 884/A 884M, Class A, Type 1 coated, [as-drawn, plain] [deformed]-steel wire, with less than 2 percent damaged coating in each 12-inch (300-mm) wire length.

        - Plain-Steel Welded-Wire Reinforcement: ASTM A 1064/A 1064M, plain, fabricated from as-drawn steel wire into flat sheets.

        - Deformed-Steel Welded-Wire Reinforcement: ASTM A 1064/A 1064M, flat sheet.

        - Galvanized-Steel Welded-Wire Reinforcement: ASTM A 1064/A 1064M, plain, fabricated from galvanized-steel wire into flat sheets.

        - Epoxy-Coated Welded-Wire Reinforcement: ASTM A 884/A 884M, Class A coated, Type 1, [plain] [deformed] steel.

      - REINFORCEMENT ACCESSORIES

Insert other products for dowels or dowel sleeves if required. These include circular and rectangular plastic dowel sleeves, square dowels, and plastic-surfaced or reinforced-paper-covered dowels.

        - Joint Dowel Bars: ASTM A 615/A 615M, Grade 60 (Grade 420), plain-steel bars, cut true to length with ends square and free of burrs.

        - Epoxy-Coated Joint Dowel Bars: ASTM A 615/A 615M, Grade 60 (Grade 420), plain-steel bars, ASTM A 775/A 775M epoxy coated.

        - Epoxy Repair Coating: Liquid, two-part, epoxy repair coating; compatible with epoxy coating on reinforcement and complying with ASTM A 775/A 775M.

        - Zinc Repair Material: ASTM A 780/A 780M.

        - Bar Supports: Bolsters, chairs, spacers, and other devices for spacing, supporting, and fastening reinforcing bars and welded-wire reinforcement in place. Manufacture bar supports from steel wire, plastic, or precast concrete according to CRSI's "Manual of Standard Practice," of greater compressive strength than concrete and as follows:

Retain one or more of three subparagraphs below; revise to suit Project.

          - For concrete surfaces exposed to view, where legs of wire bar supports contact forms, use CRSI Class 1 plastic-protected steel wire or CRSI Class 2 stainless-steel bar supports.

          - For epoxy-coated reinforcement, use epoxy-coated or other dielectric-polymer-coated wire bar supports.

          - For zinc-coated reinforcement, use galvanized wire or dielectric-polymer-coated wire bar supports.

Insert mechanical splices and connections for steel reinforcement here if required.

      - CONCRETE MATERIALS

        - Regional Materials: Concrete shall be manufactured within 500 miles (800 km) of Project site from aggregates[ and cementitious materials] that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

"Regional Materials" Paragraph below applies to LEED 2009 CI Credit MR 5, Option 1.

        - Regional Materials: Concrete shall be manufactured within 500 miles (800 km) of Project site.

        - Source Limitations: Obtain each type or class of cementitious material of the same brand from the same manufacturer's plant, obtain aggregate from single source, and obtain admixtures from single source from single manufacturer.

        - Cementitious Materials:

Retain type and color of portland cement from options in "Portland Cement" Subparagraph below.

          - Portland Cement: ASTM C 150/C 150M, [Type I] [Type II] [Type I/II] [Type III] [Type V], [gray] [white].

Retain supplementary cementing materials in "Fly Ash" and "Slag Cement" subparagraphs below if permitted. Ready-mix-concrete manufacturer blends these materials with portland cement. Fly ash, slag cement, or pozzolanic materials may slow rate of concrete strengthening and affect color uniformity. Class F fly ash is more readily available than Class C fly ash.

          - Fly Ash: ASTM C 618, [Class F] [Class F or C].

          - Slag Cement: ASTM C 989/C 989M, Grade 100 or 120.

Retain "Blended Hydraulic Cement" Subparagraph below if factory-blended hydraulic cement is permitted; verify availability of options before specifying. Fly ash, slag cement, or pozzolanic materials in the nonportland cement part of blended hydraulic cement may slow rate of concrete strengthening and affect color uniformity. Insert ASTM C 1157 if acceptable.

          - Blended Hydraulic Cement: ASTM C 595/C 595M, [Type IS, portland blast-furnace slag] [Type IP, portland-pozzolan] [Type IL, portland-limestone] [Type IT, ternary blended] cement.

Silica fume in "Silica Fume" Subparagraph below is most often used in high-strength concrete and in special applications, such as bridge decks, to enhance durability by lowering permeability of concrete. ACI 301 (ACI 301M) identifies silica fume as a cementitious material.

          - Silica Fume: ASTM C 1240, amorphous silica.

Retain class of aggregate from options in "Normal-Weight Aggregates" Paragraph below or revise to suit Project. ASTM C 33/C 33M limits deleterious substances in coarse aggregate, depending on climate severity and in-service location of concrete. Classes in first set of options are ASTM C 33/C 33M default classes for concrete exposed to weather for Severe, Moderate, and Negligible weathering regions, respectively. Revise first two options to Class 4S or 4M if concrete is exposed to frequent wetting. Retain last option if damage caused by concrete expansion from alkali silica or alkali carbonate reactions is anticipated.

        - Normal-Weight Aggregates: ASTM C 33/C 33M, [Class 3S] [Class 3M] [Class 1N] <Insert class> coarse aggregate or better, graded. Provide aggregates from a single source[ with documented service record data of at least 10 years' satisfactory service in similar applications and service conditions using similar aggregates and cementitious materials].

Retain coarse-aggregate size from three options in "Maximum Coarse-Aggregate Size" Subparagraph below; insert gradation requirements if preferred. Aggregate size limits relate to spacing of steel reinforcement, depth of slab, or thickness of concrete member.

          - Maximum Coarse-Aggregate Size: [1-1/2 inches (38 mm)] [1 inch (25 mm)] [3/4 inch (19 mm)] <Insert dimension> nominal.

Retain "Fine Aggregate" Subparagraph below if optional restriction for fine aggregate in ASTM C 33/C 33M is required.

          - Fine Aggregate: Free of materials with deleterious reactivity to alkali in cement.

Retain "Lightweight Aggregate" Paragraph below if using lightweight aggregate for structural lightweight concrete. Retain size limit from four options below.

        - Lightweight Aggregate: ASTM C 330/C 330M, [1-inch (25-mm)] [3/4-inch (19-mm)] [1/2-inch (13-mm)] [3/8-inch (10-mm)] nominal maximum aggregate size.

        - Air-Entraining Admixture: ASTM C 260/C 260M.

        - Chemical Admixtures: Certified by manufacturer to be compatible with other admixtures and that do not contribute water-soluble chloride ions exceeding those permitted in hardened concrete. Do not use calcium chloride or admixtures containing calcium chloride.

Retain one or more chemical admixtures from "Water-Reducing Admixture," "Retarding Admixture," "Water-Reducing and Retarding Admixture," "High-Range, Water-Reducing Admixture," "High-Range, Water-Reducing and Retarding Admixture," and "Plasticizing and Retarding Admixture" subparagraphs below.

          - Water-Reducing Admixture: ASTM C 494/C 494M, Type A.

          - Retarding Admixture: ASTM C 494/C 494M, Type B.

          - Water-Reducing and Retarding Admixture: ASTM C 494/C 494M, Type D.

          - High-Range, Water-Reducing Admixture: ASTM C 494/C 494M, Type F.

          - High-Range, Water-Reducing and Retarding Admixture: ASTM C 494/C 494M, Type G.

          - Plasticizing and Retarding Admixture: ASTM C 1017/C 1017M, Type II.

Retain "Set-Accelerating Corrosion-Inhibiting Admixture" Paragraph below if set-accelerating corrosion inhibitors are required. Set-accelerating products are usually calcium nitrite-based admixtures and comply with ASTM C 494/C 494M, Type C.

        - Set-Accelerating Corrosion-Inhibiting Admixture: Commercially formulated, anodic inhibitor or mixed cathodic and anodic inhibitor; capable of forming a protective barrier and minimizing chloride reactions with steel reinforcement in concrete and complying with ASTM C 494/C 494M, Type C.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - BASF Corporation; Construction Systems.

            - Euclid Chemical Company (The); an RPM company.

            - Grace Construction Products; W.R. Grace & Co. -- Conn.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

Retain "Non-Set-Accelerating Corrosion-Inhibiting Admixture" Paragraph below if corrosion inhibitors that do not affect concrete setting time are required.

        - Non-Set-Accelerating Corrosion-Inhibiting Admixture: Commercially formulated, non-set-accelerating, anodic inhibitor or mixed cathodic and anodic inhibitor; capable of forming a protective barrier and minimizing chloride reactions with steel reinforcement in concrete.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - BASF Corporation; Construction Systems.

            - Cortec Corporation.

            - Grace Construction Products; W.R. Grace & Co. -- Conn.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

Retain "Color Pigment" Paragraph below for integrally colored concrete.

        - Color Pigment: ASTM C 979/C 979M, synthetic mineral-oxide pigments[ or colored water-reducing admixtures]; color stable,[ free of carbon black,] nonfading, and resistant to lime and other alkalis.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Alabama Pigments Company, LLC.

            - BASF Corporation; Construction Systems.

            - Bon Tool Co.

            - Brickform; a division of Solomon Colors.

            - Butterfield Color.

            - Davis Colors.

            - Decosup Inc.

            - Dynamic Color Solutions, Inc.

            - Euclid Chemical Company (The); an RPM company.

            - Hoover Color Corporation.

            - Lambert Corporation.

            - LANXESS Corporation.

            - Matcrete Inc.

            - NewLook International, Inc.

            - Proline Concrete Tools, Inc.

            - QC Construction Products.

            - Rockwood Pigments NA, Inc.

            - Scofield, L. M. Company.

            - Solomon Colors, Inc.

            - Southern Color N.A., Inc.; a division of Rockwood Pigments.

            - Specialty Concrete Products, Inc.

            - Stampcrete International, Ltd.

            - SureCrete Design Products.

            - <Insert manufacturer’s name>.

Retain one of three options in "Color" Subparagraph below.

          - Color: [As indicated by manufacturer's designation] [Match Architect's sample] [As selected by Architect from manufacturer's full range].

Delete “Integral Waterproofing Admixtures” Paragraph below when using “Moxie Shield 1500 Penetrating Sealer.”

        - Integral Waterproofing Admixtures: ASTM C494, Type S; complex catalyzed hydrous silicate, water and vapor proofing liquid admixture.

          - Basis-of-Design Product: Subject to compliance with requirements, provide Moxie International Inc.; Moxie Shield 1800 Admixture, P.O. Box 838 Loomis, CA 95650; Contact Manufacturer’s representative: P:916-251-0825, F: 877-330-1930 Email: info@moxieshield.com, or comparable product by one of the following:

            - <Insert manufacturer’s name>.

          - Properties:

            - Water/Cement Ratio: Maximum 0.52.

            - Water Vapor Transmission:  Less than 0.1 perms (5.7 g/Pa·s·m2).

Subparagraph below applies to the permeability of saturated porous materials.

            - Water Seepage or Permeability: Not to exceed 7.00 x 10-9 cm/s at 50 psi (2.3 x 10-10 ft/s).

        - Water: ASTM C 94/C 94M[ and potable].

      - FIBER REINFORCEMENT

Retain one of two "Carbon-Steel Fiber" paragraphs below if using steel-fiber reinforcement. Retain length of fiber from first set of options and the ratio of length to effective diameter from second set of options for aspect ratio.

        - Carbon-Steel Fiber: ASTM A 820/A 820M, Type 1, cold-drawn wire, deformed, minimum of [1.5 inches (38 mm)] [2 inches (50 mm)] [2.4 inches (60 mm)] <Insert dimension> long, and aspect ratio of [35 to 40] [45 to 50] [60 to 65] <Insert ratio>.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Bekaert.

            - Euclid Chemical Company (The); an RPM company.

            - Nycon, Inc.

            - Propex Operating Company, LLC.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

        - Carbon-Steel Fiber: ASTM A 820/A 820M, Type 2, cut sheet, deformed, minimum of [1.5 inches (38 mm)] [2 inches (50 mm)] [2.4 inches (60 mm)] <Insert dimension> long, and aspect ratio of [35 to 40] [45 to 50] [60 to 65] <Insert ratio>.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Fibercon International, Inc.

            - Nycon, Inc.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

Retain one of two "Synthetic Micro-Fiber" paragraphs below if using synthetic micro-fiber reinforcement. Revise fiber type if inserting polyester or nylon fibers. Monofilament fibers help reduce plastic shrinkage cracking. Manufacturers claim fibrillated fibers also improve hardened concrete properties.

        - Synthetic Micro-Fiber: Monofilament polypropylene micro-fibers engineered and designed for use in concrete, complying with ASTM C 1116/C 1116M, Type III, [1/2 to 1-1/2 inches (13 to 38 mm)] [1 to 2-1/4 inches (25 to 57 mm)] <Insert dimensions> long.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Euclid Chemical Company (The); an RPM company.

            - FORTA Corporation.

            - Grace Construction Products; W.R. Grace & Co. -- Conn.

            - Nycon, Inc.

            - Propex Operating Company, LLC.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

        - Synthetic Micro-Fiber: Fibrillated polypropylene micro-fibers engineered and designed for use in concrete, complying with ASTM C 1116/C 1116M, Type III, [1/2 to 1-1/2 inches (13 to 38 mm)] [1 to 2-1/4 inches (25 to 57 mm)] <Insert dimensions> long.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Euclid Chemical Company (The); an RPM company.

            - FORTA Corporation.

            - Grace Construction Products; W.R. Grace & Co. -- Conn.

            - Nycon, Inc.

            - Propex Operating Company, LLC.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

Manufacturers claim macro-fiber reinforcement can be used for crack control and may substitute for wire mesh and some light steel-reinforcement bar configurations in slabs-on-ground and composite slabs. The quantity of fiber required to be inserted into the concrete is calculated by a structural engineer based on criteria furnished by the fiber manufacturer.

        - Synthetic Macro-Fiber: Polyolefin macro-fibers engineered and designed for use in concrete, complying with ASTM C 1116/C 1116M, Type III, [1 to 2-1/4 inches (25 to 57 mm)] <Insert dimensions> long.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Euclid Chemical Company (The); an RPM company.

            - FORTA Corporation.

            - Grace Construction Products; W.R. Grace & Co. -- Conn.

            - Nycon, Inc.

            - Propex Operating Company, LLC.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

      - WATERSTOPS

        - Flexible Rubber Waterstops: CE CRD-C 513,[ with factory-installed metal eyelets,] for embedding in concrete to prevent passage of fluids through joints. Factory fabricate corners, intersections, and directional changes.

          - Manufacturers: Subject to compliance with requirements, provide products by the following:

            - Williams Products, Inc.

            - <Insert manufacturer’s name>.

Retain profile from options in "Profile" Subparagraph below. Insert others if required.

          - Profile: [Flat dumbbell with center bulb] [Flat dumbbell without center bulb] [Ribbed with center bulb] [Ribbed without center bulb] [As indicated] <Insert profile>.

          - Dimensions: [4 inches by 3/16 inch thick (100 mm by 4.75 mm thick)] [6 inches by 3/8 inch thick (150 mm by 10 mm thick)] [9 inches by 3/8 inch thick (225 mm by 10 mm thick)] <Insert dimensions>; nontapered.

        - Chemically Resistant Flexible Waterstops: Thermoplastic elastomer rubber waterstops[ with factory-installed metal eyelets], for embedding in concrete to prevent passage of fluids through joints; resistant to oils, solvents, and chemicals. Factory fabricate corners, intersections, and directional changes.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - JP Specialties, Inc.

            - Sika Corporation.

            - <Insert manufacturer’s name>.

Retain profile from options in "Profile" Subparagraph below. Insert others if required.

          - Profile: [Flat dumbbell with center bulb] [Flat dumbbell without center bulb] [Ribbed with center bulb] [Ribbed without center bulb] [As indicated] <Insert profile>.

          - Dimensions: [4 inches by 3/16 inch thick (100 mm by 4.75 mm thick)] [6 inches by 3/16 inch thick (150 mm by 4.75 mm thick)] [6 inches by 3/8 inch thick (150 mm by 10 mm thick)] [9 inches by 3/16 inch thick (225 mm by 4.75 mm thick)] [9 inches by 3/8 inch thick (225 mm by 10 mm thick)] <Insert dimensions>; nontapered.

        - Flexible PVC Waterstops: CE CRD-C 572,[ with factory-installed metal eyelets,] for embedding in concrete to prevent passage of fluids through joints. Factory fabricate corners, intersections, and directional changes.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - BoMetals, Inc.

            - Paul Murphy Plastics Company.

            - Sika Greenstreak.

            - Vinylex Waterstop & Accessories.

            - <Insert manufacturer’s name>.

Retain profile from options in "Profile" Subparagraph below. Insert others if required.

          - Profile: [Flat dumbbell with center bulb] [Flat dumbbell without center bulb] [Ribbed with center bulb] [Ribbed without center bulb] [As indicated] <Insert profile>.

          - Dimensions: [4 inches by 3/16 inch thick (100 mm by 4.75 mm thick)] [6 inches by 3/8 inch thick (150 mm by 10 mm thick)] [9 inches by 3/8 inch thick (225 mm by 10 mm thick)] <Insert dimensions>; nontapered.

        - Self-Expanding Butyl Strip Waterstops: Manufactured rectangular or trapezoidal strip, butyl rubber with sodium bentonite or other hydrophilic polymers, for adhesive bonding to concrete, 3/4 by 1 inch (19 by 25 mm).

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Barrier-Bac; Inteplast Group, Ltd.

            - Carlisle Coatings & Waterproofing Inc.

            - CETCO, a Minerals Technologies company.

            - Concrete Sealants Inc.

            - Henry Company, Sealants Division.

            - JP Specialties, Inc.

            - Sika Greenstreak.

            - <Insert manufacturer’s name>.

        - Self-Expanding Rubber Strip Waterstops: Manufactured rectangular or trapezoidal strip, bentonite-free hydrophilic polymer-modified chloroprene rubber, for adhesive bonding to concrete, 3/8 by 3/4 inch (10 by 19 mm).

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Adeka Ultra Seal/OCM, Inc.

            - CETCO, a Minerals Technologies company.

            - Grace Construction Products; W.R. Grace & Co. -- Conn.

            - Sika Greenstreak.

            - <Insert manufacturer’s name>.

      - VAPOR RETARDERS

Retain one "Sheet Vapor Retarder" Paragraph below if a nonbituminous water vapor retarder is required.

Retain option and insert water-vapor permeance in first "Sheet Vapor Retarder" Paragraph below if requiring less than the 0.3 perms permitted by ASTM E 1745. See the Evaluations.

        - Sheet Vapor Retarder: ASTM E 1745, Class A[, except with maximum water-vapor permeance of <Insert rating>]. Include manufacturer's recommended adhesive or pressure-sensitive tape.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Barrier-Bac; Inteplast Group, Ltd.

            - Fortifiber Building Systems Group.

            - Grace Construction Products; W.R. Grace & Co. -- Conn.

            - Insulation Solutions, Inc.

            - Poly-America, L.P.

            - Raven Industries, Inc.

            - Reef Industries, Inc.

            - Stego Industries, LLC.

            - Tex-Trude, Inc.

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

Retain option and insert water-vapor permeance in first "Sheet Vapor Retarder" Paragraph below if requiring less than the 0.3 perms permitted by ASTM E 1745. See the Evaluations.

        - Sheet Vapor Retarder: ASTM E 1745, Class B[, except with maximum water-vapor permeance of <Insert rating>]. Include manufacturer's recommended adhesive or pressure-sensitive tape.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Fortifiber Building Systems Group.

            - Reef Industries, Inc.

            - <Insert manufacturer’s name>.

Retain option and insert water-vapor permeance in first "Sheet Vapor Retarder" Paragraph below if requiring less than the 0.3 perms permitted by ASTM E 1745. See the Evaluations.

        - Sheet Vapor Retarder: ASTM E 1745, Class C[, except with maximum water-vapor permeance of <Insert rating>]. Include manufacturer's recommended adhesive or pressure-sensitive joint tape.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Insulation Solutions, Inc.

            - Raven Industries, Inc.

            - Reef Industries, Inc.

            - Stego Industries, LLC.

            - Tex-Trude, Inc.

            - <Insert manufacturer’s name>.

Retain "Sheet Vapor Retarder" Paragraph below if generic polyethylene, rather than compliance with ASTM E 1745, is permitted.

        - Sheet Vapor Retarder: Polyethylene sheet, ASTM D 4397, not less than 10 mils (0.25 mm) thick.

Retain "Bituminous Vapor Retarder" Paragraph below if bituminous vapor retarder is required.

        - Bituminous Vapor Retarder: 110-mil- (2.8-mm-) thick, semiflexible, seven-ply sheet membrane consisting of reinforced core and carrier sheet with fortified asphalt layers, protective weathercoating, and removable plastic release liner. Furnish manufacturer's accessories, including bonding asphalt, pointing mastics, and self-adhering joint tape.

          - Manufacturers: Subject to compliance with requirements, provide products by the following:

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

          - Water-Vapor Permeance: 0.0011 grains/h x sq. ft. x inches Hg (0.063 ng/Pa x s x sq. m); ASTM E 154.

          - Tensile Strength: 140 lbf/inch (24.5 kN/m); ASTM E 154.

          - Puncture Resistance: 90 lbf (400N); ASTM E 154.

      - FLOOR AND SLAB TREATMENTS

Retain this article if one or more floor and slab treatments are required.

        - Slip-Resistive Emery Aggregate Finish: Factory-graded, packaged, rustproof, nonglazing, abrasive, crushed emery aggregate containing not less than 50 percent aluminum oxide and not less than 20 percent ferric oxide; unaffected by freezing, moisture, and cleaning materials with 100 percent passing [3/8-inch (9.5-mm)] [No. 4 (4.75-mm)] [No. 8 (2.36-mm)] <Insert size or gradation> sieve.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Anti-Hydro International, Inc.

            - Dayton Superior.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - <Insert manufacturer’s name>.

        - Slip-Resistive Aluminum Granule Finish: Factory-graded, packaged, rustproof, nonglazing, abrasive aggregate of not less than 95 percent fused aluminum-oxide granules.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Anti-Hydro International, Inc.

            - BASF Corporation; Construction Systems.

            - L&M Construction Chemicals, Inc.

            - <Insert manufacturer’s name>.

Delete “Emery Dry-Shake Floor Hardener” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Emery Dry-Shake Floor Hardener: [Pigmented] [Unpigmented], factory-packaged, dry combination of portland cement, graded emery aggregate, and plasticizing admixture; with emery aggregate consisting of no less than 60 percent of total aggregate content.

Retain one of three options in "Color" Subparagraph below if retaining first option in "Emery Dry-Shake Floor Hardener" Paragraph above.

          - Color: [As indicated by manufacturer's designation] [Match Architect's sample] [As selected by Architect from manufacturer's full range].

        - Metallic Dry-Shake Floor Hardener: [Pigmented] [Unpigmented], factory-packaged, dry combination of portland cement, graded metallic aggregate, rust inhibitors, and plasticizing admixture; with metallic aggregate consisting of no less than 65 percent of total aggregate content.

Retain one of three options in "Color" Subparagraph below if retaining first option in "Metallic Dry-Shake Floor Hardener" Paragraph above.

          - Color: [As indicated by manufacturer's designation] [Match Architect's sample] [As selected by Architect from manufacturer's full range].

Retain "Unpigmented Mineral Dry-Shake Floor Hardener" Paragraph below if unpigmented mineral dry-shake floor hardeners are required. Delete “Unpigmented Mineral Dry-Shake Floor Hardener” Paragraph below when using “Moxie Shield 1800 Admixture.” Verify suitability with manufacturer if air content of concrete exceeds 3 percent.

        - Unpigmented Mineral Dry-Shake Floor Hardener: Factory-packaged dry combination of portland cement, graded quartz aggregate, and plasticizing admixture.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - BASF Corporation; Construction Systems.

            - Dayton Superior.

            - Euclid Chemical Company (The); an RPM company.

            - Kaufman Products, Inc.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - Scofield, L. M. Company.

            - SpecChem, LLC.

            - <Insert manufacturer’s name>.

Retain "Pigmented Mineral Dry-Shake Floor Hardener" Paragraph below if pigmented mineral dry-shake floor hardeners are required. Verify suitability with manufacturer if air content of concrete exceeds 3 percent.

        - Pigmented Mineral Dry-Shake Floor Hardener: Factory-packaged, dry combination of portland cement, graded quartz aggregate, color pigments, and plasticizing admixture. Use color pigments that are finely ground, nonfading mineral oxides interground with cement.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Anti-Hydro International, Inc.

            - BASF Corporation; Construction Systems.

            - Bon Tool Co.

            - Brickform; a division of Solomon Colors.

            - Butterfield Color.

            - Dayton Superior.

            - Decosup Inc.

            - Dynamic Color Solutions, Inc.

            - Euclid Chemical Company (The); an RPM company.

            - H&C Concrete Care Products.

            - Kaufman Products, Inc.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - Proline Concrete Tools, Inc.

            - QC Construction Products.

            - Scofield, L. M. Company.

            - SpecChem, LLC.

            - Specialty Concrete Products, Inc.

            - Stampcrete International, Ltd.

            - SuperStone, Inc.

            - SureCrete Design Products.

            - <Insert manufacturer’s name>.

Retain one of three options in "Color" Subparagraph below.

          - Color: [As indicated by manufacturer's designation] [Match Architect's sample] [As selected by Architect from manufacturer's full range].

      - LIQUID FLOOR TREATMENTS

Penetrating liquid floor treatment in "Penetrating Liquid Floor Treatment" Paragraph below is commonly applied to harden and densify floors of warehouses and distribution facilities, imparting a clear satin sheen to finished floor. Pigmented products may also be available. Although formulations vary, manufacturers claim these nonfluosilicate liquids improve abrasion and chemical resistance and dustproof concrete surface. When approved by manufacturers, these products may be installed over mineral dry-shake floor hardeners or integrally colored concrete. Delete “Penetrating Liquid Floor Treatments” Paragraph below when using “Moxie Shield 1800 Admixture.” Surface adhered Liquid Floor Treatments are acceptable for cosmetically exposed concrete.

        - Penetrating Liquid Floor Treatment: Clear, chemically reactive, waterborne solution of inorganic silicate or siliconate materials and proprietary components; odorless; that penetrates, hardens, and densifies concrete surfaces.

          - Basis-of-Design Product: Subject to compliance with requirements, provide Moxie International Inc.; Moxie Shield 1500 Concrete Sealer or Moxie Shield MFSII Flooring Sealer, P.O. Box 838 Loomis, CA 95650; Contact Manufacturer’s representative: P:916-251-0825, F: 877-330-1930 Email: info@moxieshield.com, or comparable product by one of the following:

            - <Insert manufacturer’s name>.

          - Products shall comply with the requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

      - CURING MATERIALS

Evaporation retarders temporarily reduce moisture loss from concrete surfaces awaiting finishing in hot, dry, and windy conditions. Evaporation retarders are not curing compounds. Delete “Evaporation Retarder” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Evaporation Retarder: Waterborne, monomolecular film forming, manufactured for application to fresh concrete.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - BASF Corporation; Construction Systems.

            - Bon Tool Co.

            - Brickform; a division of Solomon Colors.

            - ChemMasters, Inc.

            - Dayton Superior.

            - Euclid Chemical Company (The); an RPM company.

            - Kaufman Products, Inc.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - Nox-Crete Products Group.

            - Sika Corporation.

            - SpecChem, LLC.

            - TK Products.

            - Vexcon Chemicals Inc.

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

Retain curing aids and materials from remaining paragraphs.

        - Absorptive Cover: AASHTO M 182, Class 2, burlap cloth made from jute or kenaf, weighing approximately 9 oz./sq. yd. (305 g/sq. m) when dry.

        - Moisture-Retaining Cover: ASTM C 171, polyethylene film or white burlap-polyethylene sheet.

        - Water: Potable.

Retain "Clear, Waterborne, Membrane-Forming Curing Compound" Paragraph below if a dissipating-type, waterborne, membrane-forming curing compound is required. Although the EPA mandates maximum VOC emissions of 350 g/L for curing compounds, verify VOC emission limits of authorities having jurisdiction. If slow breakdown of curing membrane could interfere with bonding of floor coverings, retain "Removal" Subparagraph in "Concrete Protecting and Curing" Article in Part 3. Delete “Clear, Waterborne, Membrane-Forming Curing Compound” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Clear, Waterborne, Membrane-Forming Curing Compound: ASTM C 309, Type 1, Class B, dissipating.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Anti-Hydro International, Inc.

            - BASF Corporation; Construction Systems.

            - ChemMasters, Inc.

            - Dayton Superior.

            - Euclid Chemical Company (The); an RPM company.

            - Kaufman Products, Inc.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Nox-Crete Products Group.

            - Right Pointe.

            - SpecChem, LLC.

            - TK Products.

            - Vexcon Chemicals Inc.

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

Retain "Clear, Waterborne, Membrane-Forming Curing Compound" Paragraph below if a nondissipating-type, waterborne, membrane-forming curing compound with minimal solids content is required. Although the EPA mandates maximum VOC emissions of 350 g/L for curing compounds, verify VOC emission limits of authorities having jurisdiction. Retain option if applicable. Delete “Clear, Waterborne, Membrane-Forming Curing Compound” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Clear, Waterborne, Membrane-Forming Curing Compound: ASTM C 309, Type 1, Class B, nondissipating[, certified by curing compound manufacturer to not interfere with bonding of floor covering].

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Anti-Hydro International, Inc.

            - BASF Corporation; Construction Systems.

            - ChemMasters, Inc.

            - Cresset Chemical Company.

            - Dayton Superior.

            - Euclid Chemical Company (The); an RPM company.

            - Kaufman Products, Inc.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - Nox-Crete Products Group.

            - SpecChem, LLC.

            - TK Products.

            - Vexcon Chemicals Inc.

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

Retain "Clear, Waterborne, Membrane-Forming Curing Compound" Paragraph below if a nondissipating-type, waterborne, membrane-forming curing compound with a higher solids content is required. This product will partially seal the concrete. Although the EPA mandates maximum VOC emissions of 350 g/L for curing compounds, verify VOC emission limits of authorities having jurisdiction. Retain option if applicable. Delete “Clear, Waterborne, Membrane-Forming Curing Compound” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Clear, Waterborne, Membrane-Forming Curing Compound: ASTM C 309, Type 1, Class B, 18 to 25 percent solids, nondissipating[, certified by curing compound manufacturer to not interfere with bonding of floor covering].

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - AWRC Corporation.

            - BASF Corporation; Construction Systems.

            - ChemMasters, Inc.

            - Dayton Superior.

            - Euclid Chemical Company (The); an RPM company.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - Nox-Crete Products Group.

            - SpecChem, LLC.

            - Vexcon Chemicals Inc.

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

Retain "Clear, Solvent-Borne, Membrane-Forming Curing and Sealing Compound" Paragraph below if a clear, nonyellowing, solvent-borne, membrane-forming curing and sealing compound is required. Although the EPA mandates maximum VOC emissions of 700 g/L for curing and sealing compounds, verify VOC emission limits of authorities having jurisdiction. Delete “Clear, Solvent-Borne, Membrane-Forming Curing Compound” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Clear, Solvent-Borne, Membrane-Forming Curing and Sealing Compound: ASTM C 1315, Type 1, Class A.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - BASF Corporation; Construction Systems.

            - ChemMasters, Inc.

            - Dayton Superior.

            - Euclid Chemical Company (The); an RPM company.

            - Kaufman Products, Inc.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - Nox-Crete Products Group.

            - Right Pointe.

            - SpecChem, LLC.

            - TK Products.

            - Vexcon Chemicals Inc.

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

          - Products shall comply with the requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain "Clear, Waterborne, Membrane-Forming Curing and Sealing Compound" Paragraph below if a clear, nonyellowing, waterborne, membrane-forming curing and sealing compound is required. Although the EPA mandates maximum VOC emissions of 700 g/L for curing and sealing compounds, verify VOC emission limits of authorities having jurisdiction. Delete “Clear, Waterborne, Membrane-Forming Curing and Sealing Compound” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Clear, Waterborne, Membrane-Forming Curing and Sealing Compound: ASTM C 1315, Type 1, Class A.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - AWRC Corporation.

            - BASF Corporation; Construction Systems.

            - ChemMasters, Inc.

            - Dayton Superior.

            - Euclid Chemical Company (The); an RPM company.

            - Kaufman Products, Inc.

            - L&M Construction Chemicals, Inc.

            - Lambert Corporation.

            - Metalcrete Industries.

            - Right Pointe.

            - SpecChem, LLC.

            - TK Products.

            - Vexcon Chemicals Inc.

            - W. R. Meadows, Inc.

            - <Insert manufacturer’s name>.

          - Products shall comply with the requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

      - RELATED MATERIALS

Retain one or all options in "Expansion- and Isolation-Joint-Filler Strips" Paragraph below. Joint-filler strips are used in floor isolation joints.

        - Expansion- and Isolation-Joint-Filler Strips: [ASTM D 1751, asphalt-saturated cellulosic fiber] [or] [ASTM D 1752, cork or self-expanding cork].

Retain one of two options in "Semirigid Joint Filler" Paragraph below if semirigid joint filler is required to fill joints and support edges of trafficked contraction and construction joints.

        - Semirigid Joint Filler: Two-component, semirigid, 100 percent solids, [epoxy resin with a Type A shore durometer hardness of 80] [aromatic polyurea with a Type A shore durometer hardness range of 90 to 95] according to ASTM D 2240.

Bonding agent in "Bonding Agent" Paragraph below may be used directly from container or as an admixture in cement or sand-cement slurries and rubbing grout.

        - Bonding Agent: ASTM C 1059/C 1059M, Type II, nonredispersible, acrylic emulsion or styrene butadiene.

        - Epoxy Bonding Adhesive: ASTM C 881, two-component epoxy resin, capable of humid curing and bonding to damp surfaces, of class suitable for application temperature and of grade to suit requirements, and as follows:

Retain types from two options in subparagraph below based on service loadings.

          - [Types I and II, nonload bearing] [Types IV and V, load bearing], for bonding hardened or freshly mixed concrete to hardened concrete.

Retain "Reglets" Paragraph below if reglets are not specified elsewhere. Coordinate product requirements with Section 076200 "Sheet Metal Flashing and Trim" or Section 077100 "Roof Specialties" or in other Sections where reglets are supplied as auxiliary products with waterproofing or roofing membrane flashings.

        - Reglets: Fabricate reglets of not less than 0.022-inch- (0.55-mm-) thick, galvanized-steel sheet. Temporarily fill or cover face opening of reglet to prevent intrusion of concrete or debris.

        - Dovetail Anchor Slots: Hot-dip galvanized-steel sheet, not less than 0.034 inch (0.85 mm) thick, with bent tab anchors. Temporarily fill or cover face opening of slots to prevent intrusion of concrete or debris.

      - REPAIR MATERIALS

Retain "Repair Underlayment" Paragraph below as a repair material for floor and slab areas beneath floor coverings.

        - Repair Underlayment: Cement-based, polymer-modified, self-leveling product that can be applied in thicknesses from 1/8 inch (3.2 mm) and that can be feathered at edges to match adjacent floor elevations.

          - Cement Binder: ASTM C 150/C 150M, portland cement or hydraulic or blended hydraulic cement as defined in ASTM C 219.

          - Primer: Product of underlayment manufacturer recommended for substrate, conditions, and application.

          - Aggregate: Well-graded, washed gravel, 1/8 to 1/4 inch (3.2 to 6 mm) or coarse sand as recommended by underlayment manufacturer.

          - Compressive Strength: Not less than [4100 psi (29 MPa)] <Insert strength> at 28 days when tested according to ASTM C 109/C 109M.

Retain "Repair Overlayment" Paragraph below as a repair material for floor or slab areas remaining exposed and not receiving floor coverings.

        - Repair Overlayment: Cement-based, polymer-modified, self-leveling product that can be applied in thicknesses from 1/4 inch (6.4 mm) and that can be filled in over a scarified surface to match adjacent floor elevations.

          - Cement Binder: ASTM C 150/C 150M, portland cement or hydraulic or blended hydraulic cement as defined in ASTM C 219.

          - Primer: Product of topping manufacturer recommended for substrate, conditions, and application.

          - Aggregate: Well-graded, washed gravel, 1/8 to 1/4 inch (3.2 to 6 mm) or coarse sand as recommended by topping manufacturer.

          - Compressive Strength: Not less than [5000 psi (34.5 MPa)] <Insert strength> at 28 days when tested according to ASTM C 109/C 109M.

      - CONCRETE MIXTURES, GENERAL

        - Prepare design mixtures for each type and strength of concrete, proportioned on the basis of laboratory trial mixture or field test data, or both, according to ACI 301 (ACI 301M).

          - Use a qualified independent testing agency for preparing and reporting proposed mixture designs based on laboratory trial mixtures.

Retain first option in "Cementitious Materials" Paragraph below if required for replacing part of the portland cement, which would otherwise be used in concrete, with other cementitious materials. Retain second option if limiting percentage of cementitious materials that can replace portland cement. Neither ACI 301 (ACI 301M) nor ACI 318 (ACI 318M) limit amount of cementitious materials that can replace portland cement unless concrete is exposed to deicing chemicals. Identify parts of building or structure affected by these limits unless extending them to all concrete.

        - Cementitious Materials:[ Use fly ash, pozzolan, slag cement, and silica fume as needed to reduce the total amount of portland cement, which would otherwise be used, by not less than 40 percent.] [ Limit percentage, by weight, of cementitious materials other than portland cement in concrete as follows:]

Percentages in six subparagraphs below repeat ACI 301 (ACI 301M) limits for concrete exposed to deicing chemicals. Revise to suit Project. Fly ash may be added to concrete at maximum rate of no more than 20 percent replacement by weight of scheduled amount of cement when using “Moxie Shield 1800 Admixture.”

          - Fly Ash: 25 percent.

          - Combined Fly Ash and Pozzolan: 25 percent.

          - Slag Cement: 50 percent.

          - Combined Fly Ash or Pozzolan and Slag Cement: 50 percent portland cement minimum, with fly ash or pozzolan not exceeding 25 percent.

Retain "Silica Fume," "Combined Fly Ash, Pozzolans, and Silica Fume," and "Combined Fly Ash or Pozzolans, Slag Cement, and Silica Fume" subparagraphs below if silica fume is permitted. Limits of silica fume alone or in combination with other cementitious materials below are based on ACI 301 (ACI 301M) and ACI 318 (ACI 318M).

          - Silica Fume: 10 percent.

          - Combined Fly Ash, Pozzolans, and Silica Fume: 35 percent with fly ash or pozzolans not exceeding 25 percent and silica fume not exceeding 10 percent.

          - Combined Fly Ash or Pozzolans, Slag Cement, and Silica Fume: 50 percent with fly ash or pozzolans not exceeding 25 percent and silica fume not exceeding 10 percent.

Retain appropriate option in first paragraph below for chloride limits. Identify portions of building with different limits if required. Percentages below repeat ACI 301 (ACI 301M) limits, respectively, for prestressed (post-tensioned) concrete, reinforced concrete exposed to chloride, reinforced concrete that is not dry or protected from moisture, and reinforced concrete that is dry or protected from moisture. ACI 301 (ACI 301M) and ACI 318 (ACI 318M) express this percentage by weight of cement, not cementitious material.

        - Limit water-soluble, chloride-ion content in hardened concrete to [0.06] [0.15] [0.30] [1.00] <Insert number> percent by weight of cement.

        - Admixtures: Use admixtures according to manufacturer's written instructions.

Revise four subparagraphs below to suit Project; delete if not required.

          - Use [water-reducing] [high-range water-reducing] [or] [plasticizing] admixture in concrete, as required, for placement and workability.

          - Use water-reducing and -retarding admixture when required by high temperatures, low humidity, or other adverse placement conditions.

          - Use water-reducing admixture in pumped concrete, concrete for heavy-use industrial slabs and parking structure slabs, concrete required to be watertight, and concrete with a w/c ratio below 0.50.

Insert locations and dosage of corrosion-inhibiting admixture to subparagraph below if required.                 Delete subparagraph below when using “Moxie Shield 1800 Admixture.”

          - Use corrosion-inhibiting admixture in concrete mixtures where indicated.

Retain "Color Pigment" Paragraph below if integrally colored concrete is required, and indicate locations here or on Drawings.

        - Color Pigment: Add color pigment to concrete mixture according to manufacturer's written instructions and to result in hardened concrete color consistent with approved mockup.

      - CONCRETE MIXTURES FOR BUILDING ELEMENTS

This article contains examples of building elements that often need different concrete mixtures. Revise, consolidate, or add other building elements if more concrete mixtures are required.

Consider inserting minimum cementitious material content for mix designs.

        - Footings: Normal-weight concrete.

Retain strength from first five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project. Coordinate compressive strength with w/c ratio if concrete is subject to special exposure conditions or sulfate exposure as identified in ACI 318 (ACI 318M).

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] [As indicated] <Insert strength> at 28 days.

Retain one option in "Maximum W/C Ratio" Subparagraph below, revise subparagraph to suit Project, or delete subparagraph if in-service durability conditions are benign and limits on w/c ratio are not required. Coordinate w/c ratio with compressive strength. See the Evaluations for discussion.

          - Maximum W/C Ratio: [0.50] [0.45] [0.40] <Insert number>.

Retain one of three options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)] [8 inches (200 mm) for concrete with verified slump of 2 to 4 inches (50 to 100 mm) before adding high-range water-reducing admixture or plasticizing admixture] <Insert dimension>, plus or minus 1 inch (25 mm).

Retain one or both "Air Content" subparagraphs below. Percentages in options are default air contents required by ACI 301 (ACI 301M) for severe exposure.

          - Air Content: [5.5] <Insert number> percent, plus or minus 1.5 percent at point of delivery for 1-1/2-inch (38-mm) nominal maximum aggregate size.

          - Air Content: [6] <Insert number> percent, plus or minus 1.5 percent at point of delivery for [1-inch (25-mm)] [3/4-inch (19-mm)] nominal maximum aggregate size.

        - Foundation Walls: Normal-weight concrete.

Retain strength from five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project. Coordinate compressive strength with w/c ratio if concrete is subject to special exposure conditions or sulfate exposure as identified in ACI 318 (ACI 318M).

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] [As indicated] <Insert strength> at 28 days.

Retain w/c ratio from three options in "Maximum W/C Ratio" Subparagraph below, revise to suit Project, or delete if in-service durability conditions are benign and limits on w/c ratio are not required. Coordinate w/c ratio with compressive strength. See the Evaluations for discussion.

          - Maximum W/C Ratio: [0.50] [0.45] [0.40] <Insert number>.

Retain slump limit from three options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)] [8 inches (200 mm) for concrete with verified slump of 2 to 4 inches (50 to 100 mm) before adding high-range water-reducing admixture or plasticizing admixture] <Insert dimension>, plus or minus 1 inch (25 mm).

Retain one or both "Air Content" subparagraphs below. Percentages in options are default air contents required by ACI 301 (ACI 301M) for severe exposure.

          - Air Content: [5.5] <Insert number> percent, plus or minus 1.5 percent at point of delivery for 1-1/2-inch (38-mm) nominal maximum aggregate size.

          - Air Content: [6] <Insert number> percent, plus or minus 1.5 percent at point of delivery for [1-inch (25-mm)] [3/4-inch (19-mm)] nominal maximum aggregate size.

        - Slabs-on-Grade: Normal-weight concrete.

Retain strength from five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project.

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] [As indicated] <Insert strength> at 28 days.

Retain w/c ratio from three options in "Maximum W/C Ratio" Subparagraph below, revise to suit Project, or delete if in-service durability conditions are benign and limits on w/c ratio are not required. Coordinate w/c ratio with compressive strength. See the Evaluations for discussion.

          - Maximum W/C Ratio: [0.50] [0.45] [0.40] <Insert number>.

Retain one of three options in "Minimum Cementitious Materials Content" Subparagraph below or revise to suit Project. Options are based on minimum requirements set by ACI 301 (ACI 301M) for floors and relate to nominal maximum aggregate sizes 1-1/2 inches, 1 inch, and 3/4 inch (38, 25, and 19 mm), respectively.

          - Minimum Cementitious Materials Content: [470 lb/cu. yd. (279 kg/cu. m)] [520 lb/cu. yd. (309 kg/cu. m)] [540 lb/cu. yd. (320 kg/cu. m)].

Retain slump limit from two options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)], plus or minus 1 inch (25 mm).

Retain one or more "Air Content" subparagraphs below. Percentages in options in first two subparagraphs are default air contents required by ACI 301 (ACI 301M) for severe exposure.

          - Air Content: [5.5] <Insert number> percent, plus or minus 1.5 percent at point of delivery for 1-1/2-inch (38-mm) nominal maximum aggregate size.

          - Air Content: [6] <Insert number> percent, plus or minus 1.5 percent at point of delivery for [1-inch (25-mm)] [3/4-inch (19-mm)] nominal maximum aggregate size.

Air content in "Air Content" Subparagraph below is maximum recommended by ACI 302.1R for trowel-finished floors.

          - Air Content: Do not allow air content of trowel-finished floors to exceed 3 percent.

Insert w/c ratio here if slab-on-grade is subject to special exposure conditions or injurious sulfate exposure.

Retain "Steel-Fiber Reinforcement" Subparagraph below if steel-fiber reinforcement is used. Indicate location, on Drawings, of concrete using steel fiber. Revise application rate to suit Project.

          - Steel-Fiber Reinforcement: Add to concrete mixture, according to manufacturer's written instructions, at a rate of [50 lb/cu. yd. (29.7 kg/cu. m)] <Insert weight>.

Synthetic-micro-fiber dosage rates in "Synthetic Micro-Fiber" Subparagraph below reflect typical recommendations of manufacturers. Retain first option for minimum dosage of synthetic micro-fiber used for reducing plastic shrinkage cracking. Retain second option or increase dosage for synthetic micro-fiber used for improving hardened concrete properties.

          - Synthetic Micro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [1.0 lb/cu. yd. (0.60 kg/cu. m)] [1.5 lb/cu. yd. (0.90 kg/cu. m)] <Insert dosage>.

Synthetic-macro-fiber dosage rates in "Synthetic Macro-Fiber" Subparagraph below are examples only; verify minimum dosage rates with manufacturer.

          - Synthetic Macro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [4.0 lb/cu. yd. (2.4 kg/cu. m)] [5 lb/cu. yd. (3 kg/cu. m)] <Insert dosage>.

Retain "Suspended Slabs" Paragraph below if normal-weight concrete is used. Suspended slabs include formed concrete slabs, post-tensioned concrete slabs, and composite or noncomposite concrete slabs on metal deck, classified by ACI 302.1R as single-course floors or base slabs of two-course floors. If Project has more than one type of suspended slab with different properties, indicate location of each on Drawings.

        - Suspended Slabs: Normal-weight concrete.

Retain strength from five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project.

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] <Insert strength> [As indicated] at 28 days.

Retain w/c ratio from three options in "Maximum W/C Ratio" Subparagraph below, revise to suit Project, or delete if in-service durability conditions are benign and limits on w/c ratio are not required. Coordinate w/c ratio with compressive strength. See the Evaluations for discussion.

          - Maximum W/C Ratio: [0.50] [0.45] [0.40] <Insert number>.

Retain one of three options in "Minimum Cementitious Materials Content" Subparagraph below or revise to suit Project. Options are based on minimum requirements set by ACI 301 (ACI 301M) for floors and relate to nominal maximum aggregate sizes 1-1/2 inches, 1 inch, and 3/4 inch (38, 25, and 19 mm), respectively.

          - Minimum Cementitious Materials Content: [470 lb/cu. yd. (279 kg/cu. m)] [520 lb/cu. yd. (309 kg/cu. m)] [540 lb/cu. yd. (320 kg/cu. m)].

Retain slump limit from two options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)], plus or minus 1 inch (25 mm).

Retain one or more "Air Content" subparagraphs below. Percentages in options in first two subparagraphs are default air contents required by ACI 301 (ACI 301M) for severe exposure.

          - Air Content: [5.5] <Insert number> percent, plus or minus 1.5 percent at point of delivery for 1-1/2-inch (38-mm) nominal maximum aggregate size.

          - Air Content: [6] <Insert number> percent, plus or minus 1.5 percent at point of delivery for [1-inch (25-mm)] [3/4-inch (19-mm)] nominal maximum aggregate size.

Air content in "Air Content" Subparagraph below is maximum recommended by ACI 302.1R for trowel-finished floors.

          - Air Content: Do not allow air content of trowel-finished floors to exceed 3 percent.

Insert w/c ratio here if elevated slabs are subject to special exposure conditions.

Retain "Steel-Fiber Reinforcement" Subparagraph below if steel-fiber reinforcement is used. Indicate location, on Drawings, of concrete using steel fiber. Revise application rate to suit Project.

          - Steel-Fiber Reinforcement: Add to concrete mixture, according to manufacturer's written instructions, at a rate of [50 lb/cu. yd. (29.7 kg/cu. m)] <Insert weight>.

Synthetic-micro-fiber dosage rates in "Synthetic Micro-Fiber" Subparagraph below reflect typical recommendations of manufacturers. Retain first option for minimum dosage of synthetic micro-fiber used for reducing plastic shrinkage cracking. Retain second option or increase dosage for synthetic micro-fiber used for improving hardened concrete properties.

          - Synthetic Micro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [1.0 lb/cu. yd. (0.60 kg/cu. m)] [1.5 lb/cu. yd. (0.90 kg/cu. m)] <Insert dosage>.

Synthetic-macro-fiber dosage rates in "Synthetic Macro-Fiber" Subparagraph below are examples only; verify minimum dosage rates by structural analysis and with manufacturer.

          - Synthetic Macro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [4.0 lb/cu. yd. (2.4 kg/cu. m)] [5 lb/cu. yd. (3 kg/cu. m)] <Insert dosage>.

Retain "Suspended Slabs" Paragraph below if normal-weight structural concrete is not used. Coordinate requirements with lightweight aggregate supplier, structural engineer, and, if applicable, UL design limits.

        - Suspended Slabs: Lightweight concrete.

Retain strength from five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project.

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] <Insert strength> [As indicated] at 28 days.

Retain one of three options in "Calculated Equilibrium Unit Weight" Subparagraph below or revise values or unit weight terminology. "Calculated equilibrium unit weight" is the basis preferred by the Expanded Shale Clay and Slate Institute rather than "maximum air dry unit weight," which is included in ACI 301 (ACI 301M) for measuring unit weight.

          - Calculated Equilibrium Unit Weight: [115 lb/cu. ft. (1842 kg/cu. m)] [110 lb/cu. ft. (1762 kg/cu. m)] [105 lb/cu. ft. (1682 kg/cu. m)], plus or minus 3 lb/cu. ft. (48.1 kg/cu. m) as determined by ASTM C 567/C 567M.

Retain slump limit from two options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)], plus or minus 1 inch (25 mm).

Retain one or more "Air Content" subparagraphs below. Percentages in first two subparagraphs are default air contents required by ACI 301 (ACI 301M) for lightweight concrete subject to freezing and thawing, severe weather, or deicer chemicals.

          - Air Content: 6 percent, plus or minus 2 percent at point of delivery for nominal maximum aggregate size greater than 3/8 inch (10 mm).

          - Air Content: 7 percent, plus or minus 2 percent at point of delivery for nominal maximum aggregate size 3/8 inch (10 mm) or less.

Air content in "Air Content" Subparagraph below is maximum recommended by ACI 302.1R for trowel-finished floors.

          - Air Content: Do not allow air content of trowel-finished floors to exceed 3 percent.

Retain "Steel-Fiber Reinforcement" Subparagraph below if steel-fiber reinforcement is used. Indicate location, on Drawings, of concrete using steel fiber. Revise application rate to suit Project.

          - Steel-Fiber Reinforcement: Add to concrete mixture, according to manufacturer's written instructions, at a rate of [50 lb/cu. yd. (29.7 kg/cu. m)] <Insert weight>.

Synthetic-micro-fiber dosage rates in "Synthetic Micro-Fiber" Subparagraph below reflect typical recommendations of manufacturers. Retain first option for minimum dosage of synthetic micro-fiber used for reducing plastic shrinkage cracking. Retain second option or increase dosage for synthetic micro-fiber used for improving hardened concrete properties.

          - Synthetic Micro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [1.0 lb/cu. yd. (0.60 kg/cu. m)] [1.5 lb/cu. yd. (0.90 kg/cu. m)] <Insert dosage>.

Synthetic-macro-fiber dosage rates in "Synthetic Macro-Fiber" Subparagraph below are examples only; verify minimum dosage rates by structural analysis and with manufacturer.

          - Synthetic Macro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [4.0 lb/cu. yd. (2.4 kg/cu. m)] [5 lb/cu. yd. (3 kg/cu. m)] <Insert dosage>.

Retain "Concrete Toppings" Paragraph below for concrete toppings or concrete underbeds on a base concrete slab or on structural precast concrete.

        - Concrete Toppings: Normal-weight concrete.

Retain strength from five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project.

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] <Insert strength> [As indicated] at 28 days.

Retain one of three options in "Minimum Cementitious Materials Content" Subparagraph below or revise to suit Project. Options are based on minimum requirements set by ACI 301 (ACI 301M) for floors and relate to nominal maximum aggregate sizes 1-1/2 inches, 1 inch, and 3/4 inch (38, 25, and 19 mm), respectively.

          - Minimum Cementitious Materials Content: [470 lb/cu. yd. (279 kg/cu. m)] [520 lb/cu. yd. (309 kg/cu. m)] [540 lb/cu. yd. (320 kg/cu. m)].

Retain slump limit from two options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)], plus or minus 1 inch (25 mm).

Retain one or more "Air Content" subparagraphs below. Percentages in options in first two subparagraphs are default air contents required by ACI 301 (ACI 301M) for severe exposure.

          - Air Content: [5.5] <Insert number> percent, plus or minus 1.5 percent at point of delivery for 1-1/2-inch (38-mm) nominal maximum aggregate size.

          - Air Content: [6] <Insert number> percent, plus or minus 1.5 percent at point of delivery for [1-inch (25-mm)] [3/4-inch (19-mm)] nominal maximum aggregate size.

Air content in "Air Content" Subparagraph below is maximum recommended by ACI 302.1R for trowel-finished toppings.

          - Air Content: Do not allow air content of trowel-finished toppings to exceed 3 percent.

Retain "Steel-Fiber Reinforcement" Subparagraph below if steel-fiber reinforcement is used. Indicate location, on Drawings, of concrete using steel fiber. Revise application rate to suit Project.

          - Steel-Fiber Reinforcement: Add to concrete mixture, according to manufacturer's written instructions, at a rate of [50 lb/cu. yd. (29.7 kg/cu. m)] <Insert weight>.

Synthetic-micro-fiber dosage rates in "Synthetic Micro-Fiber" Subparagraph below reflect typical recommendations of manufacturers. Retain first option for minimum dosage of synthetic micro-fiber used for reducing plastic shrinkage cracking. Retain second option or increase dosage for synthetic micro-fiber used for improving hardened concrete properties.

          - Synthetic Micro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [1.0 lb/cu. yd. (0.60 kg/cu. m)] [1.5 lb/cu. yd. (0.90 kg/cu. m)] <Insert dosage>.

Synthetic-macro-fiber dosage rates in "Synthetic Macro-Fiber" Subparagraph below are examples only; verify minimum dosage rates with manufacturer.

          - Synthetic Macro-Fiber: Uniformly disperse in concrete mixture at manufacturer's recommended rate, but not less than a rate of [4.0 lb/cu. yd. (2.4 kg/cu. m)] [5 lb/cu. yd. (3 kg/cu. m)] <Insert dosage>.

        - Building Frame Members: Normal-weight concrete.

Retain strength from five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project. Coordinate compressive strength with w/c ratio if concrete is subject to special exposure conditions or sulfate exposure as identified in ACI 318 (ACI 318M).

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] <Insert strength> [As indicated] at 28 days.

Retain w/c ratio from three options in "Maximum W/C Ratio" Subparagraph below, revise to suit Project, or delete if in-service durability conditions are benign and limits on w/c ratio are not required. Coordinate w/c ratio with compressive strength. See the Evaluations for discussion.

          - Maximum W/C Ratio: [0.50] [0.45] [0.40] <Insert number>.

Retain slump limit from three options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)] [8 inches (200 mm) for concrete with verified slump of 2 to 4 inches (50 to 100 mm) before adding high-range water-reducing admixture or plasticizing admixture] <Insert dimension>, plus or minus 1 inch (25 mm).

Retain one or both "Air Content" subparagraphs below. Percentages in options are default air contents required by ACI 301 (ACI 301M) for severe exposure.

          - Air Content: [5.5] <Insert number> percent, plus or minus 1.5 percent at point of delivery for 1-1/2-inch (38-mm) nominal maximum aggregate size.

          - Air Content: [6] <Insert number> percent, plus or minus 1.5 percent at point of delivery for [1-inch (25-mm)] [3/4-inch (19-mm)] nominal maximum aggregate size.

        - Building Walls: Normal-weight concrete.

Retain strength from five options in "Minimum Compressive Strength" Subparagraph below or revise to suit Project. Coordinate compressive strength with w/c ratio if concrete is subject to special exposure conditions or sulfate exposure as identified in ACI 318 (ACI 318M).

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] <Insert strength> [As indicated] at 28 days.

Retain w/c ratio from three options in "Maximum W/C Ratio" Subparagraph below, revise to suit Project, or delete if in-service durability conditions are benign and limits on w/c ratio are not required. Coordinate w/c ratio with compressive strength. See the Evaluations for discussion.

          - Maximum W/C Ratio: [0.50] [0.45] [0.40] <Insert number>.

Retain slump limit from three options in "Slump Limit" Subparagraph below or revise to suit Project.

          - Slump Limit: [4 inches (100 mm)] [5 inches (125 mm)] [8 inches (200 mm) for concrete with verified slump of 2 to 4 inches (50 to 100 mm) before adding high-range water-reducing admixture or plasticizing admixture] <Insert dimension>, plus or minus 1 inch (25 mm).

Retain one or both "Air Content" subparagraphs below. Percentages in options are default air contents required by ACI 301 (ACI 301M) for severe exposure.

          - Air Content: [5.5] <Insert number> percent, plus or minus 1.5 percent at point of delivery for 1-1/2-inch (38-mm) nominal maximum aggregate size.

          - Air Content: [6] <Insert number> percent, plus or minus 1.5 percent at point of delivery for [1-inch (25-mm)] [3/4-inch (19-mm)] nominal maximum aggregate size.

      - FABRICATING REINFORCEMENT

        - Fabricate steel reinforcement according to CRSI's "Manual of Standard Practice."

      - CONCRETE MIXING

Retain option in "Ready-Mixed Concrete" Paragraph below if steel or synthetic fibers are required.

        - Ready-Mixed Concrete: Measure, batch, mix, and deliver concrete according to ASTM C 94/C 94M[ and ASTM C 1116/C 1116M], and furnish batch ticket information.

          - When air temperature is between 85 and 90 deg F (30 and 32 deg C), reduce mixing and delivery time from 1-1/2 hours to 75 minutes; when air temperature is above 90 deg F (32 deg C), reduce mixing and delivery time to 60 minutes.

Retain "Project-Site Mixing" Paragraph below if Project-site mixing is permitted. ACI 301 (ACI 301M) applies measuring, batching, and mixing requirements from ASTM C 94/C 94M to Project-site mixing.

        - Project-Site Mixing: Measure, batch, and mix concrete materials and concrete according to ASTM C 94/C 94M. Mix concrete materials in appropriate drum-type batch machine mixer.

          - For mixer capacity of 1 cu. yd. (0.76 cu. m) or smaller, continue mixing at least 1-1/2 minutes, but not more than 5 minutes after ingredients are in mixer, before any part of batch is released.

          - For mixer capacity larger than 1 cu. yd. (0.76 cu. m), increase mixing time by 15 seconds for each additional 1 cu. yd. (0.76 cu. m).

          - Provide batch ticket for each batch discharged and used in the Work, indicating Project identification name and number, date, mixture type, mixture time, quantity, and amount of water added. Record approximate location of final deposit in structure.

- EXECUTION

      - FORMWORK INSTALLATION

        - Design, erect, shore, brace, and maintain formwork, according to ACI 301 (ACI 301M), to support vertical, lateral, static, and dynamic loads, and construction loads that might be applied, until structure can support such loads.

        - Construct formwork so concrete members and structures are of size, shape, alignment, elevation, and position indicated, within tolerance limits of ACI 117 (ACI 117M).

        - Limit concrete surface irregularities, designated by ACI 347 as abrupt or gradual, as follows:

Retain surface classes, usually two or more, in two subparagraphs below. See discussion in "Formwork" Article in the Evaluations. Coordinate with rough- and smooth-formed finishes in "Finishing Formed Surfaces" Article.

          - [Class A, 1/8 inch (3.2 mm)] <Insert dimension> for smooth-formed finished surfaces.

          - [Class B, 1/4 inch (6 mm)] [Class C, 1/2 inch (13 mm)] [Class D, 1 inch (25 mm)] <Insert dimension> for rough-formed finished surfaces.

        - Construct forms tight enough to prevent loss of concrete mortar.

        - Construct forms for easy removal without hammering or prying against concrete surfaces. Provide crush or wrecking plates where stripping may damage cast-concrete surfaces. Provide top forms for inclined surfaces steeper than 1.5 horizontal to 1 vertical.

          - Install keyways, reglets, recesses, and the like, for easy removal.

          - Do not use rust-stained steel form-facing material.

        - Set edge forms, bulkheads, and intermediate screed strips for slabs to achieve required elevations and slopes in finished concrete surfaces. Provide and secure units to support screed strips; use strike-off templates or compacting-type screeds.

        - Provide temporary openings for cleanouts and inspection ports where interior area of formwork is inaccessible. Close openings with panels tightly fitted to forms and securely braced to prevent loss of concrete mortar. Locate temporary openings in forms at inconspicuous locations.

Retain one of two options in first paragraph below. ACI 301 (ACI 301M) requires chamfers unless otherwise specified.

        - [Chamfer] [Do not chamfer] exterior corners and edges of permanently exposed concrete.

        - Form openings, chases, offsets, sinkages, keyways, reglets, blocking, screeds, and bulkheads required in the Work. Determine sizes and locations from trades providing such items.

        - Clean forms and adjacent surfaces to receive concrete. Remove chips, wood, sawdust, dirt, and other debris just before placing concrete.

        - Retighten forms and bracing before placing concrete, as required, to prevent mortar leaks and maintain proper alignment.

        - Coat contact surfaces of forms with form-release agent, according to manufacturer's written instructions, before placing reinforcement.

      - EMBEDDED ITEM INSTALLATION

Specify embedded items and anchorage devices for other work attached to or supported by cast-in-place concrete. Insert specific requirements for installing embedded items, if any, that are part of the Work.

        - Place and secure anchorage devices and other embedded items required for adjoining work that is attached to or supported by cast-in-place concrete. Use setting drawings, templates, diagrams, instructions, and directions furnished with items to be embedded.

          - Install anchor rods, accurately located, to elevations required and complying with tolerances in Section 7.5 of AISC 303.

Retain applicable subparagraphs below and insert others if required. Revise to suit Project.

          - Install reglets to receive waterproofing and to receive through-wall flashings in outer face of concrete frame at exterior walls, where flashing is shown at lintels, shelf angles, and other conditions.

          - Install dovetail anchor slots in concrete structures as indicated.

      - REMOVING AND REUSING FORMS

Revise removal time in "General" Paragraph below if required. Period of 24 hours is halved to 12 hours in ACI 347. Commentary in ACI 318 (ACI 318M) recognizes 12 hours for concrete using regular portland cement but advises that this period may be insufficient for concrete using Type II and Type V portland cements or ASTM C 595/C 595M blended hydraulic cements, concrete with retarding admixtures, and concrete using ice during mixing.

        - General: Formwork for sides of beams, walls, columns, and similar parts of the Work that does not support weight of concrete may be removed after cumulatively curing at not less than 50 deg F (10 deg C) for [24] <Insert number> hours after placing concrete. Concrete has to be hard enough to not be damaged by form-removal operations, and curing and protection operations need to be maintained.

Retain option in first subparagraph below if adopting recommendation of ACI 347. ACI 301 (ACI 301M) requires concrete to reach its specified compressive strength.

          - Leave formwork for beam soffits, joists, slabs, and other structural elements that support weight of concrete in place until concrete has achieved[ at least 70 percent of] its 28-day design compressive strength.

          - Remove forms only if shores have been arranged to permit removal of forms without loosening or disturbing shores.

        - Clean and repair surfaces of forms to be reused in the Work. Split, frayed, delaminated, or otherwise damaged form-facing material are not acceptable for exposed surfaces. Apply new form-release agent.

        - When forms are reused, clean surfaces, remove fins and laitance, and tighten to close joints. Align and secure joints to avoid offsets. Do not use patched forms for exposed concrete surfaces unless approved by Architect.

      - SHORING AND RESHORING INSTALLATION

Review this article with structural engineer and revise if required.

        - Comply with ACI 318 (ACI 318M) and ACI 301 (ACI 301M) for design, installation, and removal of shoring and reshoring.

          - Do not remove shoring or reshoring until measurement of slab tolerances is complete.

Revise first paragraph below if setting more detailed requirements, such as a minimum number of floors.

        - In multistory construction, extend shoring or reshoring over a sufficient number of stories to distribute loads in such a manner that no floor or member will be excessively loaded or will induce tensile stress in concrete members without sufficient steel reinforcement.

        - Plan sequence of removal of shores and reshore to avoid damage to concrete. Locate and provide adequate reshoring to support construction without excessive stress or deflection.

      - VAPOR-RETARDER INSTALLATION

        - Sheet Vapor Retarders: Place, protect, and repair sheet vapor retarder according to ASTM E 1643 and manufacturer's written instructions.

          - Lap joints 6 inches (150 mm) and seal with manufacturer's recommended tape.

        - Bituminous Vapor Retarders: Place, protect, and repair bituminous vapor retarder according to manufacturer's written instructions.

      - STEEL REINFORCEMENT INSTALLATION

        - General: Comply with CRSI's "Manual of Standard Practice" for fabricating, placing, and supporting reinforcement.

          - Do not cut or puncture vapor retarder. Repair damage and reseal vapor retarder before placing concrete.

        - Clean reinforcement of loose rust and mill scale, earth, ice, and other foreign materials that reduce bond to concrete.

        - Accurately position, support, and secure reinforcement against displacement. Locate and support reinforcement with bar supports to maintain minimum concrete cover. Do not tack weld crossing reinforcing bars.

Retain subparagraph below if welding is permitted or required.

          - Weld reinforcing bars according to AWS D1.4/D 1.4M, where indicated.

        - Set wire ties with ends directed into concrete, not toward exposed concrete surfaces.

        - Install welded-wire reinforcement in longest practicable lengths on bar supports spaced to minimize sagging. Lap edges and ends of adjoining sheets at least one mesh spacing. Offset laps of adjoining sheet widths to prevent continuous laps in either direction. Lace overlaps with wire.

Retain "Epoxy-Coated Reinforcement" Paragraph below if using epoxy-coated reinforcement.

        - Epoxy-Coated Reinforcement: Repair cut and damaged epoxy coatings with epoxy repair coating according to ASTM D 3963/D 3963M. Use epoxy-coated steel wire ties to fasten epoxy-coated steel reinforcement.

Retain "Zinc-Coated Reinforcement" Paragraph below if using zinc-coated reinforcement.

        - Zinc-Coated Reinforcement: Repair cut and damaged zinc coatings with zinc repair material according to ASTM A 780/A 780M. Use galvanized-steel wire ties to fasten zinc-coated steel reinforcement.

      - JOINTS

Coordinate joint types, description, and location with Drawings. Joint types are consolidated in this article for consistency rather than for strict sequence of installation.

        - General: Construct joints true to line with faces perpendicular to surface plane of concrete.

Revise criteria for locating construction joints in "Construction Joints" Paragraph below to suit Project.

        - Construction Joints: Install so strength and appearance of concrete are not impaired, at locations indicated or as approved by Architect.

          - Place joints perpendicular to main reinforcement. Continue reinforcement across construction joints unless otherwise indicated. Do not continue reinforcement through sides of strip placements of floors and slabs.

Retain first subparagraph below if keyed joints are used. Keyed joints are used in walls and floors and between walls and slabs or footings. ACI 302.1R recommends limiting keyed joints to lightly trafficked floors, because keys may fail and lips may chip after concrete shrinks.

          - Form keyed joints as indicated. Embed keys at least 1-1/2 inches (38 mm) into concrete.

          - Locate joints for beams, slabs, joists, and girders in the middle third of spans. Offset joints in girders a minimum distance of twice the beam width from a beam-girder intersection.

          - Locate horizontal joints in walls and columns at underside of floors, slabs, beams, and girders and at the top of footings or floor slabs.

Insert spacing of construction joints in first subparagraph below if preferred.

          - Space vertical joints in walls [as indicated] <Insert spacing>. Locate joints beside piers integral with walls, near corners, and in concealed locations where possible.

Retain one of two subparagraphs below only if a bonding material is permitted.

          - Use a bonding agent at locations where fresh concrete is placed against hardened or partially hardened concrete surfaces.

          - Use epoxy-bonding adhesive at locations where fresh concrete is placed against hardened or partially hardened concrete surfaces.

Insert spacing of contraction (control) joints here or on Drawings if required. Contraction-joint spacings vary with slab thickness, aggregate size, and slump based on PCA's recommendations. Depth of joint may be varied to suit cutting method or if steel-fiber reinforcement is used.

        - Contraction Joints in Slabs-on-Grade: Form weakened-plane contraction joints, sectioning concrete into areas as indicated. Construct contraction joints for a depth equal to at least [one-fourth] <Insert depth> of concrete thickness as follows:

Retain type of joint-forming method from "Grooved Joints" and "Sawed Joints" subparagraphs below or retain both subparagraphs as Contractor's option. Insert joint spacing if not indicated on Drawings.

          - Grooved Joints: Form contraction joints after initial floating by grooving and finishing each edge of joint to a radius of 1/8 inch (3.2 mm). Repeat grooving of contraction joints after applying surface finishes. Eliminate groover tool marks on concrete surfaces.

Retain "Sawed Joints" Subparagraph below if saw cutting is permitted. Description does not distinguish conventional wet- and dry-cut saws from early-entry dry-cut saws. Timing is critical to sawed joints. Early-entry dry-cut saws are used within one to two hours of finishing concrete. To leave concrete undamaged from sawing, conventional saw cutting must be delayed, usually 4 to 12 hours, but not so long that uncontrolled cracking of concrete could occur.

          - Sawed Joints: Form contraction joints with power saws equipped with shatterproof abrasive or diamond-rimmed blades. Cut 1/8-inch- (3.2-mm-) wide joints into concrete when cutting action does not tear, abrade, or otherwise damage surface and before concrete develops random contraction cracks.

        - Isolation Joints in Slabs-on-Grade: After removing formwork, install joint-filler strips at slab junctions with vertical surfaces, such as column pedestals, foundation walls, grade beams, and other locations, as indicated.

Retain one or both of first two subparagraphs below. If both are required, indicate location of each on Drawings.

          - Extend joint-filler strips full width and depth of joint, terminating flush with finished concrete surface unless otherwise indicated.

          - Terminate full-width joint-filler strips not less than 1/2 inch (13 mm) or more than 1 inch (25 mm) below finished concrete surface where joint sealants, specified in Section 079200 "Joint Sealants," are indicated.

          - Install joint-filler strips in lengths as long as practicable. Where more than one length is required, lace or clip sections together.

Retain "Doweled Joints" Paragraph below if doweled contraction or expansion joints are used; revise if precoated dowels are required.

        - Doweled Joints: Install dowel bars and support assemblies at joints where indicated. Lubricate or asphalt coat one-half of dowel length to prevent concrete bonding to one side of joint.

      - WATERSTOP INSTALLATION

Retain "Flexible Waterstops" or "Self-Expanding Strip Waterspots" Paragraph below, depending on type of waterstop required.

        - Flexible Waterstops: Install in construction joints and at other joints indicated to form a continuous diaphragm. Install in longest lengths practicable. Support and protect exposed waterstops during progress of the Work. Field fabricate joints in waterstops according to manufacturer's written instructions.

        - Self-Expanding Strip Waterstops: Install in construction joints and at other locations indicated, according to manufacturer's written instructions, adhesive bonding, mechanically fastening, and firmly pressing into place. Install in longest lengths practicable.

      - CONCRETE PLACEMENT

        - Before placing concrete, verify that installation of formwork, reinforcement, and embedded items is complete and that required inspections are completed.

Retain one of first two paragraphs below. ACI 301 (ACI 301M) permits water to be added to concrete mixture on-site to adjust slump, up to amount allowed in design mixture.

        - Do not add water to concrete during delivery, at Project site, or during placement unless approved by Architect.

        - Before test sampling and placing concrete, water may be added at Project site, subject to limitations of ACI 301 (ACI 301M).

Retain subparagraph below if high-range water-reducing admixtures are permitted.

          - Do not add water to concrete after adding high-range water-reducing admixtures to mixture.

        - Deposit concrete continuously in one layer or in horizontal layers of such thickness that no new concrete is placed on concrete that has hardened enough to cause seams or planes of weakness. If a section cannot be placed continuously, provide construction joints as indicated. Deposit concrete to avoid segregation.

          - Deposit concrete in horizontal layers of depth not to exceed formwork design pressures and in a manner to avoid inclined construction joints.

          - Consolidate placed concrete with mechanical vibrating equipment according to ACI 301 (ACI 301M).

          - Do not use vibrators to transport concrete inside forms. Insert and withdraw vibrators vertically at uniformly spaced locations to rapidly penetrate placed layer and at least 6 inches (150 mm) into preceding layer. Do not insert vibrators into lower layers of concrete that have begun to lose plasticity. At each insertion, limit duration of vibration to time necessary to consolidate concrete and complete embedment of reinforcement and other embedded items without causing mixture constituents to segregate.

        - Deposit and consolidate concrete for floors and slabs in a continuous operation, within limits of construction joints, until placement of a panel or section is complete.

          - Consolidate concrete during placement operations, so concrete is thoroughly worked around reinforcement and other embedded items and into corners.

          - Maintain reinforcement in position on chairs during concrete placement.

          - Screed slab surfaces with a straightedge and strike off to correct elevations.

          - Slope surfaces uniformly to drains where required.

          - Begin initial floating using bull floats or darbies to form a uniform and open-textured surface plane, before excess bleedwater appears on the surface. Do not further disturb slab surfaces before starting finishing operations.

      - FINISHING FORMED SURFACES

Retain types of formed finishes required in this article. Coordinate finishes retained with finish schedule or indicate location of each finish on Drawings.

        - Rough-Formed Finish: As-cast concrete texture imparted by form-facing material with tie holes and defects repaired and patched. Remove fins and other projections that exceed specified limits on formed-surface irregularities.

          - Apply to concrete surfaces [not exposed to public view] <Insert locations>.

        - Smooth-Formed Finish: As-cast concrete texture imparted by form-facing material, arranged in an orderly and symmetrical manner with a minimum of seams. Repair and patch tie holes and defects. Remove fins and other projections that exceed specified limits on formed-surface irregularities.

Revise locations in subparagraph below to suit Project. Retain second option if additional finishing is required.

          - Apply to concrete surfaces [exposed to public view,] [to receive a rubbed finish,] [or to be covered with a coating or covering material applied directly to concrete] <Insert locations>.

If retaining "Rubbed Finish" Paragraph below, retain "Smooth-Formed Finish" Paragraph above.

        - Rubbed Finish: Apply the following to smooth-formed-finished as-cast concrete where indicated:

Retain one or more rubbed finishes in "Smooth-Rubbed Finish," "Grout-Cleaned Finish," and "Cork-Floated Finish" subparagraphs below.

          - Smooth-Rubbed Finish: Not later than one day after form removal, moisten concrete surfaces and rub with carborundum brick or another abrasive until producing a uniform color and texture. Do not apply cement grout other than that created by the rubbing process.

          - Grout-Cleaned Finish: Wet concrete surfaces and apply grout of a consistency of thick paint to coat surfaces and fill small holes. Mix 1 part portland cement to 1-1/2 parts fine sand with a 1:1 mixture of bonding admixture and water. Add white portland cement in amounts determined by trial patches, so color of dry grout matches adjacent surfaces. Scrub grout into voids and remove excess grout. When grout whitens, rub surface with clean burlap and keep surface damp by fog spray for at least 36 hours.

          - Cork-Floated Finish: Wet concrete surfaces and apply a stiff grout. Mix 1 part portland cement and 1 part fine sand with a 1:1 mixture of bonding agent and water. Add white portland cement in amounts determined by trial patches, so color of dry grout matches adjacent surfaces. Compress grout into voids by grinding surface. In a swirling motion, finish surface with a cork float.

        - Related Unformed Surfaces: At tops of walls, horizontal offsets, and similar unformed surfaces adjacent to formed surfaces, strike off smooth and finish with a texture matching adjacent formed surfaces. Continue final surface treatment of formed surfaces uniformly across adjacent unformed surfaces unless otherwise indicated.

      - FINISHING FLOORS AND SLABS

        - General: Comply with ACI 302.1R recommendations for screeding, restraightening, and finishing operations for concrete surfaces. Do not wet concrete surfaces.

Retain one or more of "Scratch Finish," "Float Finish," "Trowel Finish," "Trowel and Fine-Broom Finish," and "Slip-Resistive Finish" paragraphs below for types of slab finishes required. Coordinate slab finishes retained with finish schedule or indicate location of each finish on Drawings.

        - Scratch Finish: While still plastic, texture concrete surface that has been screeded and bull-floated or darbied. Use stiff brushes, brooms, or rakes to produce a profile amplitude of 1/4 inch (6 mm) in one direction.

Revise locations of scratch finish in subparagraph below to suit Project.

          - Apply scratch finish to surfaces [indicated] [and] [to receive concrete floor toppings] [to receive mortar setting beds for bonded cementitious floor finishes] <Insert locations>.

        - Float Finish: Consolidate surface with power-driven floats or by hand floating if area is small or inaccessible to power-driven floats. Restraighten, cut down high spots, and fill low spots. Repeat float passes and restraightening until surface is left with a uniform, smooth, granular texture.

Revise locations of float finish in subparagraph below to suit Project.

          - Apply float finish to surfaces [indicated] [to receive trowel finish] [and] [to be covered with fluid-applied or sheet waterproofing, built-up or membrane roofing, or sand-bed terrazzo] <Insert locations>.

        - Trowel Finish: After applying float finish, apply first troweling and consolidate concrete by hand or power-driven trowel. Continue troweling passes and restraighten until surface is free of trowel marks and uniform in texture and appearance. Grind smooth any surface defects that would telegraph through applied coatings or floor coverings.

Revise locations of trowel finish in first subparagraph below to suit Project.

          - Apply a trowel finish to surfaces [indicated] [exposed to view] [or] [to be covered with resilient flooring, carpet, ceramic or quarry tile set over a cleavage membrane, paint, or another thin-film-finish coating system] <Insert locations>.

          - Finish surfaces to the following tolerances, according to ASTM E 1155 (ASTM E 1155M), for a randomly trafficked floor surface:

Revise surface plane tolerances to suit Project. See the Evaluations for description of F-number system. ACI 301 (ACI 301M) suggests that all residential floors and nonresidential floors less than 10,000 sq. ft. (929 sq. m) be measured by straightedge method and that other nonresidential floors be measured by F-number system.

Retain floor flatness and levelness values required for Project from first four subparagraphs below, or revise values to suit type of floor. ACI 302.1R suggests values in first subparagraph be used for carpeted slabs; those in second and third, for thin floor coverings; and those in fourth, for very flat floors for high-speed forklifts, air pallets, and ice and roller rinks.

            - Specified overall values of flatness, F(F) 25; and of levelness, F(L) 20; with minimum local values of flatness, F(F) 17; and of levelness, F(L) 15.

            - Specified overall values of flatness, F(F) 35; and of levelness, F(L) 25; with minimum local values of flatness, F(F) 24; and of levelness, F(L) 17; for slabs-on-grade.

            - Specified overall values of flatness, F(F) 30; and of levelness, F(L) 20; with minimum local values of flatness, F(F) 24; and of levelness, F(L) 15; for suspended slabs.

            - Specified overall values of flatness, F(F) 45; and of levelness, F(L) 35; with minimum local values of flatness, F(F) 30; and of levelness, F(L) 24.

Retain straightedge method in subparagraph below if deleting F-number system above.

          - Finish and measure surface, so gap at any point between concrete surface and an unleveled, freestanding, 10-ft.- (3.05-m-) long straightedge resting on two high spots and placed anywhere on the surface does not exceed [1/4 inch (6 mm)] [3/16 inch (4.8 mm)] [1/8 inch (3.2 mm)].

        - Trowel and Fine-Broom Finish: Apply a first trowel finish to surfaces [indicated] [where ceramic or quarry tile is to be installed by either thickset or thinset method]. While concrete is still plastic, slightly scarify surface with a fine broom.

          - Comply with flatness and levelness tolerances for trowel-finished floor surfaces.

Retain "Broom Finish" Paragraph below if applicable. Broom finish is generally used on exterior concrete steps and platforms, ramps, and other surfaces subject to light foot traffic.

        - Broom Finish: Apply a broom finish to exterior concrete platforms, steps, ramps, and elsewhere as indicated.

          - Immediately after float finishing, slightly roughen trafficked surface by brooming with fiber-bristle broom perpendicular to main traffic route. Coordinate required final finish with Architect before application.

Retain "Slip-Resistive Finish" Paragraph below if applicable. This finish is generally used on interior and exterior concrete treads, platforms, and ramps subject to moderate foot traffic.

        - Slip-Resistive Finish: Before final floating, apply slip-resistive [aggregate] [aluminum granule] finish where indicated and to concrete stair treads, platforms, and ramps. Apply according to manufacturer's written instructions and as follows:

          - Uniformly spread [25 lb/100 sq. ft. (12 kg/10 sq. m)] <Insert rate> of dampened slip-resistive [aggregate] [aluminum granules] over surface in one or two applications. Tamp aggregate flush with surface, but do not force below surface.

Revise float finish in first subparagraph below to trowel finish if required.

          - After broadcasting and tamping, apply float finish.

          - After curing, lightly work surface with a steel wire brush or an abrasive stone and water to expose slip-resistive [aggregate] [aluminum granules].

Retain Dry-Shake Floor Hardener Finish Paragraph below if pigmented or unpigmented dry-shake floor hardener finish is required. Delete “Dry-Shake Floor Hardener Finish” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Dry-Shake Floor Hardener Finish: After initial floating, apply dry-shake floor hardener to surfaces according to manufacturer's written instructions and as follows:

Consult manufacturers and revise rate of application in first subparagraph below if required. This rate is usually recommended for light traffic.

          - Uniformly apply dry-shake floor hardener at a rate of [100 lb/100 sq. ft. (49 kg/10 sq. m)] <Insert rate> unless greater amount is recommended by manufacturer.

          - Uniformly distribute approximately two-thirds of dry-shake floor hardener over surface by hand or with mechanical spreader, and embed by power floating. Follow power floating with a second dry-shake floor hardener application, uniformly distributing remainder of material, and embed by power floating.

Coordinate selection of curing compounds for compatibility with dry-shake floor hardener, and revise lists of manufacturers in Part 2 accordingly if required.

          - After final floating, apply a trowel finish. Cure concrete with curing compound recommended by dry-shake floor hardener manufacturer and apply immediately after final finishing.

      - MISCELLANEOUS CONCRETE ITEM INSTALLATION

This article is an example only. Insert, revise, or delete items to suit Project.

        - Filling In: Fill in holes and openings left in concrete structures after work of other trades is in place unless otherwise indicated. Mix, place, and cure concrete, as specified, to blend with in-place construction. Provide other miscellaneous concrete filling indicated or required to complete the Work.

        - Curbs: Provide monolithic finish to interior curbs by stripping forms while concrete is still green and by steel-troweling surfaces to a hard, dense finish with corners, intersections, and terminations slightly rounded.

        - Equipment Bases and Foundations:

          - Coordinate sizes and locations of concrete bases with actual equipment provided.

          - Construct concrete bases [4 inches (100 mm)] [6 inches (150 mm)] [8 inches (200 mm)] <Insert dimension> high unless otherwise indicated, and extend base not less than 6 inches (150 mm) in each direction beyond the maximum dimensions of supported equipment unless otherwise indicated or unless required for seismic anchor support.

          - Minimum Compressive Strength: [5000 psi (34.5 MPa)] [4500 psi (31 MPa)] [4000 psi (27.6 MPa)] [3500 psi (24.1 MPa)] [3000 psi (20.7 MPa)] <Insert value> at 28 days.

          - Install dowel rods to connect concrete base to concrete floor. Unless otherwise indicated, install dowel rods on 18-inch (450-mm) centers around the full perimeter of concrete base.

          - For supported equipment, install epoxy-coated anchor bolts that extend through concrete base and anchor into structural concrete substrate.

          - Prior to pouring concrete, place and secure anchorage devices. Use setting drawings, templates, diagrams, instructions, and directions furnished with items to be embedded.

          - Cast anchor-bolt insert into bases. Install anchor bolts to elevations required for proper attachment to supported equipment.

        - Steel Pan Stairs: Provide concrete fill for steel pan stair treads, landings, and associated items. Cast-in inserts and accessories as shown on Drawings. Screed, tamp, and trowel finish concrete surfaces.

      - CONCRETE PROTECTING AND CURING

        - General: Protect freshly placed concrete from premature drying and excessive cold or hot temperatures. Comply with ACI 306.1 for cold-weather protection and ACI 301 (ACI 301) for hot-weather protection during curing.

If evaporation rate in "Evaporation Retarder" Paragraph below is exceeded, ACI 305R states that plastic shrinkage cracking is probable. See manufacturers' literature or ACI 305R for estimated moisture-loss chart relating relative humidity, air and concrete temperature, and wind velocity to rate of evaporation. Delete “Evaporation Retarder” Paragraph below when using “Moxie Shield 1800 Admixture.”

        - Evaporation Retarder: Apply evaporation retarder to unformed concrete surfaces if hot, dry, or windy conditions cause moisture loss approaching 0.2 lb/sq. ft. x h (1 kg/sq. m x h) before and during finishing operations. Apply according to manufacturer's written instructions after placing, screeding, and bull floating or darbying concrete, but before float finishing.

        - Formed Surfaces: Cure formed concrete surfaces, including underside of beams, supported slabs, and other similar surfaces. If forms remain during curing period, moist cure after loosening forms. If removing forms before end of curing period, continue curing for remainder of curing period.

        - Unformed Surfaces: Begin curing immediately after finishing concrete. Cure unformed surfaces, including floors and slabs, concrete floor toppings, and other surfaces.

        - Cure concrete according to ACI 308.1, by one or a combination of the following methods:

Retain one or more of "Moisture Curing," "Moisture-Retaining-Cover Curing," "Curing Compound," and "Curing and Sealing Compound" subparagraphs below. Restrict use of curing methods to specific locations or types of surfaces if required.

          - Moisture Curing: Keep surfaces continuously moist for not less than seven days with the following materials:

Retain first three subparagraphs below as Contractor's options unless unsuited for Project. In extreme evaporation conditions, fog mist with water only in accordance with ACI 302 concrete floor and slab construction when using “Moxie Shield 1800 Admixture.”

            - Water.

            - Continuous water-fog spray.

            - Absorptive cover, water saturated, and kept continuously wet. Cover concrete surfaces and edges with 12-inch (300-mm) lap over adjacent absorptive covers.

          - Moisture-Retaining-Cover Curing: Cover concrete surfaces with moisture-retaining cover for curing concrete, placed in widest practicable width, with sides and ends lapped at least 12 inches (300 mm), and sealed by waterproof tape or adhesive. Cure for not less than seven days. Immediately repair any holes or tears during curing period, using cover material and waterproof tape.

Retain first three subparagraphs below or revise to suit Project.

            - Moisture cure or use moisture-retaining covers to cure concrete surfaces to receive floor coverings.

            - Moisture cure or use moisture-retaining covers to cure concrete surfaces to receive penetrating liquid floor treatments.Delete “or a curing compound” in subparagraph below when using “Moxie Shield 1800 Admixture.”

            - Cure concrete surfaces to receive floor coverings with either a moisture-retaining cover [or a curing compound] that the manufacturer certifies does not interfere with bonding of floor covering used on Project.

Delete “Curing Compound” Paragraph below when using “Moxie Shield 1800 Admixture.”

          - Curing Compound: Apply uniformly in continuous operation by power spray or roller according to manufacturer's written instructions. Recoat areas subjected to heavy rainfall within three hours after initial application. Maintain continuity of coating and repair damage during curing period.

Retain "Removal" Subparagraph below if requiring removal of curing compounds that may interfere with adhesion of floor coverings. Delete “Removal” subparagraph below when using “Moxie Shield 1800 Admixture.”

            - Removal: After curing period has elapsed, remove curing compound without damaging concrete surfaces by method recommended by curing compound manufacturer[ unless manufacturer certifies curing compound does not interfere with bonding of floor covering used on Project].

Curing and sealing compound is usually for floors and slabs and may act as a permanent surface finish. Delete “Curing and Sealing Compound” Paragraph below when using “Moxie Shield 1800 Admixture.”

          - Curing and Sealing Compound: Apply uniformly to floors and slabs indicated in a continuous operation by power spray or roller according to manufacturer's written instructions. Recoat areas subjected to heavy rainfall within three hours after initial application. Repeat process 24 hours later and apply a second coat. Maintain continuity of coating and repair damage during curing period.

Delete “LIQUID FLOOR TREATMENT APPLICATION” Article below when using “Moxie Shield 1800 Admixture.”

      - LIQUID FLOOR TREATMENT APPLICATION

        - Penetrating Liquid Floor Treatment: Prepare, apply, and finish penetrating liquid floor treatment according to manufacturer's written instructions.

          - Remove curing compounds, sealers, oil, dirt, laitance, and other contaminants that impede absorption and penetration; and complete surface repairs.

Penetrating liquid floor treatment also functions as a curing aid. Coordinate with "Concrete Protecting and Curing" Article. Do not apply “Moxie Shield 1500 Penetrating Sealer” to fresh concrete (less than 28 days’ old) if a calcium chloride accelerator was used.

          - Do not apply to concrete that is less than [three] [seven] [14] [28] days' old.

Perform initial a “Water Absorption Test” pouring two to three tablespoons of water onto concrete,  surface, verifying water is absorbed in 15 to 20 seconds. If water test fails, abrade or cut surface and repeat test until it passes.

Use “Plastic Sheet Test” in conjunction with a “Dew Point Hygrometer” prior to applying “Moxie 1500 Concrete Sealer.” Do not use “Calcium Chloride Test” or the “Electrical Conductivity or Probe Test” as tests either remove moisture necessary for chemical reaction or give erroneous readings.

        - Usually delete "Sealing Coat" Paragraph below if two coats of curing and sealing compound have already been applied during curing stage. Sealing coat may be used as turnover coat, independent of means of curing, to improve appearance of an exposed concrete floor at end of Project. Sealing Coat: Uniformly apply a continuous sealing coat of curing and sealing compound to hardened concrete by power spray or roller according to manufacturer's written instructions.

      - JOINT FILLING

Retain this article if joint filling is required.

        - Prepare, clean, and install joint filler according to manufacturer's written instructions.

ACI 302.1R recommends joint filling be deferred as long as possible in concrete floors. Use of polyurea joint fillers may allow joint filling to proceed earlier; verify minimum time period with manufacturer. Typically, up to 30 percent of concrete shrinkage takes place in first month, with 80 to 90 percent during first 12 months. Revise period in subparagraph below if too short or too long. Joints must be filled before industrial floors can be placed in service.

          - Defer joint filling until concrete has aged at least [one] [six] month(s). Do not fill joints until construction traffic has permanently ceased.

        - Remove dirt, debris, saw cuttings, curing compounds, and sealers from joints; leave contact faces of joints clean and dry.

        - Install semirigid joint filler full depth in saw-cut joints and at least 2 inches (50 mm) deep in formed joints. Overfill joint and trim joint filler flush with top of joint after hardening.

      - CONCRETE SURFACE REPAIRS

This article provides basic applications for repairing concrete surfaces. Revise or delete to suit Project.

        - Defective Concrete: Repair and patch defective areas when approved by Architect. Remove and replace concrete that cannot be repaired and patched to Architect's approval.

        - Patching Mortar: Mix dry-pack patching mortar, consisting of 1 part portland cement to 2-1/2 parts fine aggregate passing a No. 16 (1.18-mm) sieve, using only enough water for handling and placing.

Insert provision for testing repair technique on a mockup or surface to be concealed later, before repairing surfaces.

        - Repairing Formed Surfaces: Surface defects include color and texture irregularities, cracks, spalls, air bubbles, honeycombs, rock pockets, fins and other projections on the surface, and stains and other discolorations that cannot be removed by cleaning.

          - Immediately after form removal, cut out honeycombs, rock pockets, and voids more than 1/2 inch (13 mm) in any dimension to solid concrete. Limit cut depth to 3/4 inch (19 mm). Make edges of cuts perpendicular to concrete surface. Clean, dampen with water, and brush-coat holes and voids with bonding agent. Fill and compact with patching mortar before bonding agent has dried. Fill form-tie voids with patching mortar or cone plugs secured in place with bonding agent.

          - Repair defects on surfaces exposed to view by blending white portland cement and standard portland cement so that, when dry, patching mortar matches surrounding color. Patch a test area at inconspicuous locations to verify mixture and color match before proceeding with patching. Compact mortar in place and strike off slightly higher than surrounding surface.

          - Repair defects on concealed formed surfaces that affect concrete's durability and structural performance as determined by Architect.

        - Repairing Unformed Surfaces: Test unformed surfaces, such as floors and slabs, for finish and verify surface tolerances specified for each surface. Correct low and high areas. Test surfaces sloped to drain for trueness of slope and smoothness; use a sloped template.

          - Repair finished surfaces containing defects. Surface defects include spalls, popouts, honeycombs, rock pockets, crazing and cracks in excess of 0.01 inch (0.25 mm) wide or that penetrate to reinforcement or completely through unreinforced sections regardless of width, and other objectionable conditions.

          - After concrete has cured at least 14 days, correct high areas by grinding.

          - Correct localized low areas during or immediately after completing surface finishing operations by cutting out low areas and replacing with patching mortar. Finish repaired areas to blend into adjacent concrete.

Retain one or both of first two subparagraphs below if applicable. First subparagraph uses an underlayment; second, a topping.

          - Correct other low areas scheduled to receive floor coverings with a repair underlayment. Prepare, mix, and apply repair underlayment and primer according to manufacturer's written instructions to produce a smooth, uniform, plane, and level surface. Feather edges to match adjacent floor elevations.

          - Correct other low areas scheduled to remain exposed with a repair topping. Cut out low areas to ensure a minimum repair topping depth of 1/4 inch (6 mm) to match adjacent floor elevations. Prepare, mix, and apply repair topping and primer according to manufacturer's written instructions to produce a smooth, uniform, plane, and level surface.

          - Repair defective areas, except random cracks and single holes 1 inch (25 mm) or less in diameter, by cutting out and replacing with fresh concrete. Remove defective areas with clean, square cuts and expose steel reinforcement with at least a 3/4-inch (19-mm) clearance all around. Dampen concrete surfaces in contact with patching concrete and apply bonding agent. Mix patching concrete of same materials and mixture as original concrete, except without coarse aggregate. Place, compact, and finish to blend with adjacent finished concrete. Cure in same manner as adjacent concrete.

          - Repair random cracks and single holes 1 inch (25 mm) or less in diameter with patching mortar. Groove top of cracks and cut out holes to sound concrete and clean off dust, dirt, and loose particles. Dampen cleaned concrete surfaces and apply bonding agent. Place patching mortar before bonding agent has dried. Compact patching mortar and finish to match adjacent concrete. Keep patched area continuously moist for at least 72 hours.

        - Perform structural repairs of concrete, subject to Architect's approval, using epoxy adhesive and patching mortar.

        - Repair materials and installation not specified above may be used, subject to Architect's approval.

      - FIELD QUALITY CONTROL

Retain "Special Inspections" or "Testing Agency" Paragraph below.

Retain first option in "Special Inspections" Paragraph below if authorities having jurisdiction require Owner to engage a special inspector. Retain last option if Owner engages testing agency, with or without a special inspector. See "Testing and Inspecting Considerations" Article in the Evaluations.

        - Special Inspections: Owner will engage a [special inspector] [and] [qualified testing and inspecting agency] to perform field tests and inspections and prepare test reports.

Retain "Testing Agency" Paragraph below if Contractor engages testing agency.

        - Testing Agency: Engage a qualified testing and inspecting agency to perform tests and inspections and to submit reports.

        - Inspections:

Retain seven subparagraphs below if special inspections are required. Items below are examples of special inspections and are based on IBC requirements; revise to insert other inspections or to suit requirements of other building codes.

          - Steel reinforcement placement.

          - Steel reinforcement welding.

          - Headed bolts and studs.

          - Verification of use of required design mixture.

          - Concrete placement, including conveying and depositing.

          - Curing procedures and maintenance of curing temperature.

          - Verification of concrete strength before removal of shores and forms from beams and slabs.

        - Concrete Tests: Testing of composite samples of fresh concrete obtained according to ASTM C 172/C 172M shall be performed according to the following requirements:

Retain one of two "Testing Frequency" subparagraphs below. First subparagraph is an example that produces more frequent testing than second subparagraph, which is the minimum required to comply with ACI 301 (ACI 301M).

          - Testing Frequency: Obtain one composite sample for each day's pour of each concrete mixture exceeding 5 cu. yd. (4 cu. m), but less than 25 cu. yd. (19 cu. m), plus one set for each additional 50 cu. yd. (38 cu. m) or fraction thereof.

          - Testing Frequency: Obtain at least one composite sample for each 100 cu. yd. (76 cu. m) or fraction thereof of each concrete mixture placed each day.

Retain first subparagraph below with either "Testing Agency" Subparagraph retained above.

            - When frequency of testing provides fewer than five compressive-strength tests for each concrete mixture, testing shall be conducted from at least five randomly selected batches or from each batch if fewer than five are used.

          - Slump: ASTM C 143/C 143M; one test at point of placement for each composite sample, but not less than one test for each day's pour of each concrete mixture. Perform additional tests when concrete consistency appears to change.

          - Air Content: ASTM C 231/C 231M, pressure method, for normal-weight concrete; [ASTM C 173/C 173M, volumetric method, for structural lightweight concrete; ]one test for each composite sample, but not less than one test for each day's pour of each concrete mixture.

          - Concrete Temperature: ASTM C 1064/C 1064M; one test hourly when air temperature is 40 deg F (4.4 deg C) and below or 80 deg F (27 deg C) and above, and one test for each composite sample.

Retain "Unit Weight" Subparagraph below if structural lightweight concrete is required.

          - Unit Weight: ASTM C 567/C 567M, fresh unit weight of structural lightweight concrete; one test for each composite sample, but not less than one test for each day's pour of each concrete mixture.

          - Compression Test Specimens: ASTM C 31/C 31M.

            - Cast and laboratory cure two sets of two standard cylinder specimens for each composite sample.

Field-cured specimens in first subparagraph below may be required to verify adequacy of curing and protection of concrete, to verify strength for tilt-up concrete and post-tensioning concrete, or to verify strength for removal of shoring and reshoring in multistory construction. Revise number of test specimens if required.

            - Cast and field cure [two] <Insert number> sets of two standard cylinder specimens for each composite sample.

Coordinate the number of compression test specimens in last subparagraph above with number of compressive-strength tests in "Compressive-Strength Tests" Subparagraph below.

          - Compressive-Strength Tests: ASTM C 39/C 39M; test one set of two laboratory-cured specimens at 7 days and one set of two specimens at 28 days.

Revise age at testing in first subparagraph below or delete if not required. Limit field testing to concrete in designated structural elements if not required throughout Project.

            - Test one set of two field-cured specimens at 7 days and one set of two specimens at 28 days.

            - A compressive-strength test shall be the average compressive strength from a set of two specimens obtained from same composite sample and tested at age indicated.

Retain first subparagraph below if field-cured specimens are required.

          - When strength of field-cured cylinders is less than 85 percent of companion laboratory-cured cylinders, Contractor shall evaluate operations and provide corrective procedures for protecting and curing in-place concrete.

          - Strength of each concrete mixture will be satisfactory if every average of any three consecutive compressive-strength tests equals or exceeds specified compressive strength and no compressive-strength test value falls below specified compressive strength by more than 500 psi (3.4 MPa).

          - Test results shall be reported in writing to Architect, concrete manufacturer, and Contractor within 48 hours of testing. Reports of compressive-strength tests shall contain Project identification name and number, date of concrete placement, name of concrete testing and inspecting agency, location of concrete batch in Work, design compressive strength at 28 days, concrete mixture proportions and materials, compressive breaking strength, and type of break for both 7- and 28-day tests.

          - Nondestructive Testing: Impact hammer, sonoscope, or other nondestructive device may be permitted by Architect but will not be used as sole basis for approval or rejection of concrete.

          - Additional Tests: Testing and inspecting agency shall make additional tests of concrete when test results indicate that slump,[ air entrainment,] compressive strengths, or other requirements have not been met, as directed by Architect. Testing and inspecting agency may conduct tests to determine adequacy of concrete by cored cylinders complying with ASTM C 42/C 42M or by other methods as directed by Architect.

          - Additional testing and inspecting, at Contractor's expense, will be performed to determine compliance of replaced or additional work with specified requirements.

          - Correct deficiencies in the Work that test reports and inspections indicate do not comply with the Contract Documents.

Retain paragraph below if measurements of floor flatness and levelness tolerances are required.

        - Measure floor and slab flatness and levelness according to ASTM E 1155 (ASTM E 1155M) within [24] [48] <Insert number> hours of finishing.

      - PROTECTION OF LIQUID FLOOR TREATMENTS

        - Protect liquid floor treatment from damage and wear during the remainder of construction period. Use protective methods and materials, including temporary covering, recommended in writing by liquid floor treatments installer.

END OF SECTION 033000